PUBLIC HEALTH COMMITTEE

COMMITTEE OF EXPERTS ON MATERIALS COMING INTO

CONTACT WITH FOOD

POLICY STATEMENT

CONCERNING

COATINGS INTENDED TO COME INTO CONTACT WITH FOODSTUFFS

Version 3 - 12.02.2009

NOTE TO THE READER

The following documents are part of the Policy statement concerning coatings intended to come into contact with foodstuffs:

- Framework Resolution ResAP (2004) 1 on coatings intended to come into contact with foodstuffs

- Technical document No. 1 – List of substances to be used in the manufacture of coatings intended to come into contact with foodstuffs (Version 3)

The documents are available on the Internet website of the Partial Agreement in the Social and Public Health Field:

www.coe.int/soc-sp

# TABLE OF CONTENTS

Page

Framework Resolution ResAP (2004) 1 on coatings intended to come into

contact with foodstuffs 	6

Technical document No. 1 – List of substances to be used in the manufacture

of coatings intended to come into contact with foodstuffs (Version 3)	11

A. List 1 of monomers	20

B. Temporary appendix to list 1 of monomers	32

C. List 1 of additives	38

D. Temporary appendix to list 1 of additives	58

FRAMEWORK RESOLUTION RESAP (2004) 1 ON COATINGS

INTENDED TO COME INTO CONTACT WITH FOODSTUFFS

FRAMEWORK RESOLUTION RESAP (2004) 1 ON COATINGS

INTENDED TO COME INTO CONTACT WITH FOODSTUFFS

(Adopted by the Committee of Ministers

on 1st December 2004 at the  907th meeting of the Ministers’ Deputies)

(Superseding Resolution AP (96) 5)

The Committee of Ministers, in its composition restricted to the Representatives of Austria, Belgium, Cyprus, Denmark, Finland, France, Germany, Ireland, Italy, Luxembourg, The Netherlands, Norway, Portugal, Slovenia, Spain, Sweden, Switzerland and the United Kingdom, member states of the Partial Agreement in the Social and Public Health Field,

Recalling Resolution (59) 23 of 16 November 1959, concerning the extension of the activities of the Council of Europe in the social and cultural fields;

Having regard to Resolution (96) 35 of 2 October 1996, whereby it revised the structures of the Partial Agreement and resolved to continue, on the basis of revised rules replacing those set out in Resolution (59) 23, the activities hitherto carried out and developed by virtue of that resolution; these being aimed in particular at:

a. raising the level of health protection of consumers in its widest sense: constant contribution to harmonising – in the field of products having a direct or indirect impact on the human food chain as well as in the field of pesticides, pharmaceuticals and cosmetics – legislation, regulations and practices governing, on the one hand, quality, efficiency and safety controls for products and, on the other hand, the safe use of toxic or noxious products;

b. integrating people with disabilities into the community: defining – and contributing to its implementation at European level – a model coherent policy for people with disabilities, which takes account simultaneously of the principles of full citizenship and independent living; contributing to the elimination of barriers to integration, whatever their nature, whether psychological, educational, family-related, cultural, social, professional, financial or architectural;

Having regard to the action carried out for several years for the purposes of harmonising their legislation in the public health field and, in particular, with regard to materials and articles intended to come into contact with foodstuffs;

Considering that coatings intended to come into contact with foodstuffs may, through migration of constituents to the foodstuffs, pose under certain conditions a risk to human health;

Noting that certain issues expressed in general terms in the Appendix to the present framework resolution need further analysis, input from other scientific projects currently carried out and appropriate innovative solutions;

Taking the view that each member state, faced with the need to introduce regulations governing this matter, would find it beneficial to harmonise such regulations at European level,

Recommends to the governments of the member states of the Partial Agreement in the Social and Public Health field to take into account in their national laws and regulations on coatings intended to come into contact with foodstuffs the principles set out hereafter.

APPENDIX TO

FRAMEWORK RESOLUTION RESAP (2004) 1 ON COATINGS

INTENDED TO COME INTO CONTACT WITH FOODSTUFFS

1. Field of application

Framework Resolution ResAP (2004) 1 on coatings intended to come into contact with foodstuffs applies to coatings which in the finished state are intended to come into contact or which are brought into contact with foodstuffs and are designed for that purpose. The following types of coating are covered:

a)  Coatings for metal packaging;

b)  Flexible packaging coatings;

c)  Heavy-duty coatings.

2. Definition

For the purpose of the framework resolution, “coatings” mean the finished material prepared mainly from organic materials applied to form a layer/film on a substrate in such a way as to create a protective layer and/or to impart technical performance.

3. Specifications

Coatings used for food contact applications under normal or foreseeable conditions of use should meet the following conditions:

3.1. they should not transfer their constituents to foodstuffs in quantities, which could  endanger human health, bring about an unacceptable change in the composition of the foodstuffs or a deterioration in the organoleptic characteristics thereof;

3.2. they should be manufactured in accordance with guidelines on good manufacturing practice for coatings intended to come into contact with foodstuffs and using substances of “Technical document No. 1 - List of substances to be used in the manufacture of coatings intended to come into contact with foodstuffs” as well as aids to polymerisation as set out in Resolution AP (92) 2 on control of aids to polymerisation (technological coadjuvants) for plastics materials and articles intended to come into contact with foodstuffs or substances of relevant national regulations, and prepared, applied and cured in strict adherence to manufacturer’s specifications, according to the conditions specified;

3.3. they should not transfer their constituents to foodstuffs in quantities exceeding 10 mg/dm2 of surface area of material or article (mg/dm2) (overall migration limit). However, this limit should be 60 mg of the constituents released per kg of foodstuff (mg/kg) in the following cases:

- articles which are containers or are comparable to containers or which can be filled, with a capacity of not less than 500 ml and not more than 10 l;

- articles which can be filled and for which it is impracticable to estimate the surface area in contact with foodstuffs;

- caps, gaskets, stoppers or other similar devices for sealing.

3.4. they should not transfer migrating components not listed in “Technical document No. 1 – List of substances to be used in the manufacture of coatings intended to come into contact with foodstuffs” which have MW  < 1000 D in quantities which could endanger human health. These non listed substances of MW < 1000 D should be subjected to appropriate risk assessment taking into account dietary exposure as well as toxicological and structure activity considerations.

###### TECHNICAL DOCUMENT No. 1

LIST OF SUBSTANCES TO BE USED IN THE MANUFACTURE OF COATINGS INTENDED TO COME INTO CONTACT WITH FOODSTUFFS

Version 3 – 12.02.2009

# 1. INTRODUCTION

1.1. The Technical document No. 1 contains the lists of monomers and additives which may be used in the manufacture of coatings intended to come into contact with foodstuffs.

The lists include :

| A. | LIST 1 OF MONOMERS : list of monomers assessed |
| --- | --- |
| B. | TEMPORARY APPENDIX TO LIST 1 OF MONOMERS : list of monomers approved by Partial Agreement member states or by FDA, applying evaluation criteria at the time of their approval |
| C. | LIST 1 OF ADDITIVES : list of additives assessed |
| D. | TEMPORARY APPENDIX TO LIST 1 OF ADDITIVES : list of additives approved by Partial Agreement member states or by FDA, applying evaluation criteria at the time of their approval |

1.2. The lists of monomers (A and B) include:

substances undergoing polymerisation, which includes polycondensation, polyaddition or any other similar process, to manufacture macromolecules,

natural or synthetic macromolecular substances used in the manufacture of modified macromolecules, if the monomers or the other starting substances required to synthesise them are not included in the list,

substances used to modify existing natural or synthetic macromolecular substances.

1.3. The lists of additives (C and D) contain:

(a)	substances which are incorporated into coating to achieve a technical effect in the finished product.  They are intended to be present in the finished articles;

(b)	substances used to provide a suitable medium in which polymerisation occurs (e.g. emulsifiers, surfactants, buffering agents etc.).

1.4. The following substances are not included even if they are intentionally used and are authorized:

(a)	salts (including double salts and acid salts) of aluminium, ammonium, calcium, iron, magnesium, potassium and sodium of authorised acids, phenols or alcohols.  However,  names containing “…acid(s), salts” appear in the lists, if the corresponding free acid(s) is (are) not mentioned;

(b)	salts (including double salts and acid salts) of zinc of authorised acids, phenols or alcohols.  For these salts a Group SML = 25 mg/kg (expressed as Zn) applies.  The same restriction for Zn applies to:

(i)	substances whose name contains “… acid(s), salts” which appear in the lists, if the

corresponding free acid(s) is (are) not mentioned,

(ii)	substances referred to in note 38 of chapter 3.

1.5. The list also does not include the following substances although they may be present:

(a)	substances which could be present in the finished product as:

- impurities in the substances used,

- reaction intermediates,

- decomposition products;

(b)	oligomers and natural or synthetic macromolecular substances as well as their mixtures, if the monomers or starting substances required to synthesise them are included in the lists;

(c)	mixtures of the authorised substances.

1.6. Substances shall be of good technical quality as regards the purity criteria.

2. INFORMATION AND ABBREVIATIONS

The lists contain the following information :

| PM/REF No | : | the EU packaging material reference number of the substance |
| --- | --- | --- |
| CAS No | : | the Chemical Abstracts Service Registry Number of the substance |
| NAME | : | the chemical name of the substance or the substance group |
| SCF-L | : | the number of the list in which the substance is classified by the Scientific Committee for food/EFSA |
| RESTRICTIONS AND/OR SPECIFICATIONS | : | Restrictions and/or specifications related to the substance |
| ADI/TDI | : | acceptable daily intake or tolerable daily intake as defined in the reports of the Scientific Committee for food/EFSA |

A number of abbreviations are used under RESTRICTIONS AND/OR SPECIFICATIONS and ADI/TDI, the meanings of which are as follows :

| ACC | Acceptable |
| --- | --- |
| DL | detection limit of the method of analysis |
| FP | finished product |
| ND | not detectable |
| NS | not specified |

| SML | specific migration limit in food or in food simulants |
| --- | --- |
| SML(T) | specific migration limit in food or in food simulants expressed as total of moiety/substance(s) indicated |
| QM | Maximum permitted quantity of the “residual” substance in the material. For the purpose of this Resolution the quantity of the substance in the material shall be determined by a validated method of analysis. If such a method does not currently exist, an analytical method with appropriate performance characteristics at the specified limit may be used, pending the development of a validated method |
| QM(T) | Maximum permitted quantity of the “residual” substance in the material expressed as total of moiety or substance(s) indicated. For the purpose of this Resolution the quantity of the substance in the material should be determined by a validated method of analysis. If such a method does not currently exist, an analytical method with appropriate performance characteristics at the specified limit may be used, pending the development of a validated method |
| QMA | Maximum permitted quantity of the “residual” substance in the finished material expressed as mg per 6 dm2 of the surface in contact with foodstuffs. For the purpose of this Resolution the quantity of the substance in the surface of the material should be determined by a validated method of analysis. If such a method does not currently exist, an analytical method with appropriate performance characteristics at the specified limit may be used, pending the development of a validated method |
| QMA(T) | Maximum permitted quantity of the “residual” substance in the material expressed as mg of total of moiety or substance(s) indicated per 6 dm2 of the surface in contact with foodstuffs. For the purpose of this Resolution the quantity of the substance in the surface of the material should be determined by a validated method of analysis. If such a method does not currently exist, an analytical method with appropriate performance characteristics at the specified limit may be used, pending the development of a validated method |

3. NOTES RELATED TO THE COLUMN "RESTRICTIONS AND/OR SPECIFICATIONS"

| (1) | Warning: there is a risk that the SML could be exceeded in fatty food simulants |
| --- | --- |
| (2) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration of the following substances mentioned as PM/REF N°: 10060 and 23920 |
| (3) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration of the following substances mentioned as PM/REF N°: 15760, 16990, 47680, 53650 and 89440 |
| (4) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration of the following substances mentioned as PM/REF N°: 19540, 19960 and 64800 |
| (5) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration of the following substances mentioned as PM/REF N°: 14200, 14230 and 41840 |
| (6) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration of the following substances mentioned as PM/REF N°: 66560 and 66580 |
| (7) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 30080, 42320, 45195, 45200, 53610, 81760, 89200 and 92030 |
| (8) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 24886, 38000, 42400, 62020, 64320, 66350, 67896, 73040, 85760, 85840, 85920 and 95725 |
| (9) | Warning: there is a risk that the migration of the substance deteriorates the organoleptic characteristics of the food in contact and then, that the finished product does not comply with the second indent of Article 2 of Directive 89/109/EEC |
| (10) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 30180, 40980, 63200, 65120, 65200, 65280, 65360, 65440 and 73120 |
| (11) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels (expressed as Iodine) of the following substances mentioned as PM/REF N°: 45200, 64320, 81680 and 86800 |
| (12) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 36720, 36800, 36840 and 92000 |
| (13) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration of the following substances mentioned as PM/REF N°: 39090 and 39120 |
| (14) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 44960, 68078, 69160, 82020 and 89170 |
| (15) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 15970, 48640, 48720, 48880, 61280, 61360 and 61600 |

| (16) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 49595, 49600, 67515, 67520 and 83599 |
| --- | --- |
| (17) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 50160, 50240, 50320, 50360, 50400, 50480, 50560, 50640, 50720, 50800, 50880, 50960, 51040 and 51120 |
| (18) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 67600, 67680 and 67760 |
| (19) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 60400, 60480 and 61440 |
| (20) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 66400 and 66480 |
| (21) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 93120 and 93280 |
| (22) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 17260, 18670, 54880 and 59280 |
| (23) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 13620, 36840, 40320 and 87040 |
| (24) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 13720 and 40580 |
| (25) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 16650 and 51570 |
| (26) | QM(T) in this specific case means that the restriction shall not be exceeded by the sum of the residual quantities of the following substances mentioned as PM/REF N°: 14950, 15700, 16240, 16570, 16600, 16630, 18640, 19110, 22332, 22420, 22570, 25210, 25240 and 25270 |
| (27) | QMA(T) in this specific case means that the restriction shall not be exceeded by the sum of the residual quantities of the following substances mentioned PM/REF N°: 10599/90A, 10599/91, 10599/92A and 10599/93 |
| (28) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 13480 and 39680 |
| (29) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 22775 and 69920 |
| (30) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 86480, 86960 and 87120 |
| (31) | Compliance testing when there is a fat contact should be performed using saturated fatty food simulants as simulant D |

| (32) | Compliance testing when there is a fat contact should be performed using isooctane as substitute of simulant D (unstable) |
| --- | --- |
| (33) | QMA(T) in this specific case means that the restriction shall not be exceeded by the sum of the residual quantities of the following substances mentioned as PM/REF N°: 14800 and 45600 |
| (34) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 55200, 55280 and 55360 |
| (35) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 25540 and 25550 |
| (36) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 10690, 10750, 10780, 10810, 10840, 11470, 11590, 11680, 11710, 11830, 11890, 11980, 31500 and 76463 |
| (37) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 20020, 20080, 20110, 20140, 20170, 20890, 21010, 21100, 21130, 21190, 21280, 21340 and 21460 |
| (38) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 81515, 96190, 96240 and 96230 as well as of salts (including double salts and acid salts) of zinc of authorised acids, phenols or alcohols. The same restriction for Zn applies to the names containing “…acid(s), salts” which appear in the lists, if the corresponding free acid(s) is (are) not mentioned |
| (39) | Migration limit might be exceeded at very high temperature |
| (40) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 38940 and 40020 |
| (41) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 47600, 67360 |
| (42) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 75100 and 75105 |
| (43) | SML(T) in this specific case means that the restriction shall not be exceeded by the sum of the migration levels of the following substances mentioned as PM/REF N°: 19150 and 19180 |

4. Annex

Specifications

Part A: General specifications

Plastic materials shall not release primary aromatic amines in a detectable quantity (DL = 0,01 mg/kg of food or food simulant).  The migration of the primary aromatic amines appearing in the lists A and C is excluded from this restriction.

Part B: Other specifications

| PM/REF N° | Other specifications |
| --- | --- |
| 11530 | Acrylic acid, 2-hydroxypropyl ester It may contain up to 25% (m/m) of acrylic acid, 2-hydroxyisopropyl ester (CAS No 002918-23-2) |
| 16690 | Divinylbenzene It may contain up to 45% (m/m) of Ethylvinylbenzene |
| 23547 | Polydimethylsiloxane (Mw > 6800) Minimum viscosity 100 x 10-6 m2/s (= 100 centistokes) at 25°C |
| 42080 | Carbon black Specifications: Toluene extractables: maximum 0,1% determined according to ISO method 6209 UV absorption of cyclohexane extract at 386 nm: < 0,02 AU for a 1 cm cell or < 0,1 AU for a 5 cm cell, determined according to a generally recognised method of analysis Benzo(a)pyrene content: max 0,25 mg/kg carbon black Maximum use level of carbon black in the polymer: 2,5% w/w |
| 72081/10 | Petroleum hydrocarbon resins (hydrogenated) Specifications: Petroleum hydrocarbon resins, hydrogenated are produced by the catalytic or thermal polymerization of dienes and olefins of the aliphatic, alicyclic and/or monobenzenoid arylalkene types from distillates of cracked petroleum stocks with a boiling range not greater than 220°C, as well as the pure monomers found in these distillation streams, subsequently followed by distillation, hydrogenation and additional processing Properties: Viscosity: > 3 Pa.s at 120°C Softening point: > 95°C as determined by ASTM Method E 28-67 Bromine number: < 40 (ASTM D1159) The colour of a 50% solution in toluene < 11 on the Gardner scale Residual aromatic monomer ≤ 50 ppm |
| 76721 | Polydimethylsiloxane (Mw > 6 800) Minimum viscosity 100 x 10-6 m2/s (= 100 centistokes) at 25°C |
| 76723 | Polydimethylsiloxane, 3-aminopropyl terminated, polymer with dicyclohexylmethane-4, 4’-diisocyanate The fraction with molecular weight below 1000 should not exceed 1.5% w/w |
| 76725 | Polydimethylsiloxane, 3-aminopropyl terminated, polymer with 1-isocyanato-3-isocyanatomethyl-3,5,5-trimethylcyclohexane The fraction with molecular weight below 1000 should not exceed 1% w/w |

| 77895 | Polyethyleneglycol (EO = 2-6) monoalkyl (C16-C18) ether The composition of the mixture is as follows: polyethyleneglycol (EO = 2-6) monoalkyl (C16-C18) ether (approximately 28%) fatty alcohols (C16-C18) (approximately 48%) ethyleneglycol monoalkyl (C16-C18) ether (approximately 24%) |
| --- | --- |
| 79600 | Polyethyleneglycol tridecyl ether phosphate Polyethyleneglycol (EO ≤ 11) tridecyl ether phosphate (mono-and dialkyl ester) with a maximum 10% content of polyethyleneglycol (EO ≤ 11) tridecylether |
| 80480 | Poly(6-morpholino-1,3,5-triazine-2,4-diyl)-[(2,2,6,6-tetramethyl-4-piperidyl)-imino]-hexamethylene-(2,2,6,6-tetramethyl-4-piperidyl)-imino- Weight average molecular weight ≥ 2400 Da. Residual content of morpholine ≤ 30 mg.kg, of N,N’-bis(2,2,6,6-tetramethylpiperidin-4-yl)hexane-1,6-diamine ≤ 15000 mg/kg, and of 2,4-dichloro-6-morpholino-1,3,5-triazine ≤ 20 mg/kg in the UV stabiliser |
| 81280 | Polyvinyl alcohol Weight average molecular weight should not be less than 2500 Da. |
| 81500 | Polyvinylpyrrolidone The substance shall meet the purity criteria established in Commission Directive 96/77/EC |
| 83595 | Reaction product of di-tert-butylphosphonite with biphenyl, obtained by condensation of 2,4-di-tert-butylphenol with Friedel Craft reaction product of phosphorous trichloride and biphenyl Composition: 4,4’-Biphenylene-bis [0,0-bis(2,4-di-tert-butylphenyl)phosphonite] (CAS No 38613-77-3) (36-46% w/w) 4,3’-Biphenylene-bis [0,0-bis(2,4-di-tert-butylphenyl)phosphonite] (CAS No 118421-00-4) (17-23% w/w) 3,3’-Biphenylene-bis[0,0-bis(2,4-di-tert-butylphenyl)phosphonite] (CAS No 118421-01-5) (1-5% w/w) 4-Biphenylene-0,0-bis(2,4-di-tert-butylphenyl)phosphonite (CAS No 91362-37-7) (11-19% w/w) Tris(2,4-di-tert-butylphenyl)phosphate (CAS No 31570-04-4) (9-18% w/w) 4,4’-Biphenylene-0,0-bis(2,4-di-tert-butylphenyl)phosphonate-0,0-bis(2,4-di-tert-butylphenyl)phosphonite (CAS No 112949-97-0) (< 5% w/w) Other specifications: Phosphor content of min. 5,4% to max. 5,9% Acid value of max. 10 mg KOH per gram Melt range of 85-110°C |
| 88640 | Soybean oil, epoxidized Oxirane < 8%, iodine number < 6 |
| 95859 | Waxes, refined, derived from petroleum based or synthetic hydrocarbon feedstocks The product should have the following specifications: Content of mineral hydrocarbons with Carbon number less than 25, not more than 5% (w/w) Viscosity not less than 11 x 10-6 m2/s (= 11 centistokes) at 100°C Average molecular weight not less than 500 |

| 95883 | White mineral oils, paraffinic derived from petroleum based hydrocarbon feedstocks The product should have the following specifications: Content of mineral hydrocarbons with Carbon number less than 25, not more than 5% (w/w) Viscosity not less than 8,5x10-6 m2/s (=8,5 centistokes) at 100°C Average molecular weight not less than 480 |
| --- | --- |

A. LIST 1 OF MONOMERS February 2009

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| --- | --- | --- | --- | --- | --- |
| 10030 | 000514-10-3 | Abietic acid | 2 |  | 1 |
| 10060 | 000075-07-0 | Acetaldehyde | 2 | SML(T) = 6 mg/kg (2) | 0.1 |
| 10090 | 000064-19-7 | Acetic acid | 1 |  | NS |
| 10120 | 000108-05-4 | Acetic acid, vinyl ester | 2 | SML = 12 mg/kg | 0.2 |
| 10599/90A | 061788-89-4 | Acids, fatty, unsaturated (C18), dimers, distilled | 3 | QMA(T) = 0.05 mg/6 dm² (27) |  |
| 10599/91 | 061788-89-4 | Acids, fatty, unsaturated (C18), dimers, non distilled | 3 | QMA(T) = 0.05 mg/6 dm² (27) |  |
| 10599/92A | 068783-41-5 | Acids, fatty, unsaturated (C18), dimers, hydrogenated, distilled | 3 | QMA(T) = 0.05 mg/6 dm² (27) |  |
| 10599/93 | 068783-41-5 | Acids, fatty, unsaturated (C18), dimers, hydrogenated, non distilled | 3 | QMA(T) = 0.05 mg/6 dm² (27) |  |
| 10630 | 000079-06-1 | Acrylamide | 4A | SML = ND (DL = 0.01 mg/kg) |  |
| 10660 | 015214-89-8 | 2-Acrylamido-2-methylpropanesulphonic acid | 3 | SML = 0.05 mg/kg |  |
| 10690 | 000079-10-7 | Acrylic acid | 2 | SML(T) = 6 mg/kg (36) | 0,1 |
| 10750 | 002495-35-4 | Acrylic acid, benzyl ester | 2 | SML(T) = 6 mg/kg (36) (as acrylic acid) | 0.1 (as acrylic acid) |
| 10780 | 000141-32-2 | Acrylic acid, n-butyl ester | 2 | SML(T) = 6 mg/kg (36) (as acrylic acid) | 0.1 (as acrylic acid) |
| 10810 | 002998-08-5 | Acrylic acid, sec-butyl ester | 2 | SML(T) = 6 mg/kg (36) (as acrylic acid) | 0.1 (as acrylic acid) |
| 10840 | 001663-39-4 | Acrylic acid, tert-butyl ester | 2 | SML(T) = 6 mg/kg (36) (as acrylic acid) | 0.1 (as acrylic acid) |
| 11245 | 002156-97-0 | Acrylic acid, dodecyl ester | 3 | SML = 0.05 mg/kg (1) |  |
| 11470 | 000140-88-5 | Acrylic acid, ethyl ester | 2 | SML(T) = 6 mg/kg (36) (as acrylic acid) | 0.1 (as acrylic acid) |
| 11500 | 000103-11-7 | Acrylic acid, 2-ethylhexyl ester | 3 | SML = 0.05 mg/kg |  |
| 11530 | 000999-61-1 | Acrylic acid, 2-hydroxypropyl ester | 3 | QMA = 0.05 mg/6 dm² for the sum of acrylic acid, 2-hydro- xypropyl ester and acrylic acid, 2-hydroxyisopropyl ester and in compliance with the specifications laid down in Annex |  |
| 11590 | 000106-63-8 | Acrylic acid, isobutyl ester | 2 | SML(T) = 6 mg/kg (36) (as acrylic acid) | 0.1 (as acrylic acid) |
| 11680 | 000689-12-3 | Acrylic acid, isopropyl ester | 2 | SML(T) = 6 mg/kg (36) (as acrylic acid) | 0.1 (as acrylic acid) |
| 11710 | 000096-33-3 | Acrylic acid, methyl ester | 2 | SML(T) = 6 mg/kg (36) (as acrylic acid) | 0.1 (as acrylic acid) |
| 11830 | 000818-61-1 | Acrylic acid, monoester with ethyleneglycol | 2 | SML(T) = 6 mg/kg (36) (as acrylic acid) | 0.1 (as acrylic acid) |
| 11890 | 002499-59-4 | Acrylic acid, n-octyl ester | 2 | SML(T) = 6 mg/kg (36) (as acrylic acid) | 0.1 (as acrylic acid) |
| 11980 | 000925-60-0 | Acrylic acid, propyl ester | 2 | SML(T) = 6 mg/kg (36) (as acrylic acid) | 0.1 (as acrylic acid) |
| 12100 | 000107-13-1 | Acrylonitrile | 4A | SML = ND (DL = 0.02 mg/kg, analytical tolerance included) |  |
| 12130 | 000124-04-9 | Adipic acid | 1 |  | 5 |
| 12280 | 002035-75-8 | Adipic anhydride | 2 |  | 5 |
| 12375 | - | Alcohols, aliphatic, monohydric, saturated, linear, primary (C4-C22) | 3 |  |  |
| 12670 | 002855-13-2 | 1-Amino-3-aminomethyl-3,5,5-trimethylcyclohexane | 2 | SML = 6 mg/kg | 0,1 |
| 12763 | 000141-43-5 | 2-Aminoethanol | 3 | SML = 0.05 mg/kg. Not for use in polymers contacting foods for which simulant D is laid down in Directive 85/572/EEC and for indirect food contact only, behind the PET layer |  |
| 12786 | 000919-30-2 | 3-Aminopropyltriethoxysilane | 3 | Residual extractable content of 3-aminopropyltriethoxysila- ne to be less than 3 mg/kg filler when used for the react- ive surface treatment of inor- ganic fillers and SML = 0.05 mg/kg when used for the sur- face treatment of materials |  |
| 12789 | 007664-41-7 | Ammonia | 1 |  | NS |
| 12820 | 000123-99-9 | Azelaic acid | 2 |  | 3 |
| 12970 | 004196-95-6 | Azelaic anhydride | 2 |  | 3 |
| 12980 | 008015-74-5 | Beechnut oil | 3 |  |  |
| 12983/1 | - | Beechnut oil fatty acids | 3 |  |  |
| (36880) | 008012-89-3 | Beeswax | 0 |  |  |
| 13000 | 001477-55-0 | 1,3-Benzenedimethanamine | 3 | SML = 0.05 mg/kg |  |
| 13090 | 000065-85-0 | Benzoic acid | 1 |  | 5 |
| 13150 | 000100-51-6 | Benzyl alcohol | 1 |  | 5 |
| 13210 | 001761-71-3 | Bis(4-aminocyclohexyl)methane | 3 | SML = 0,05 mg/kg |  |
| 13250 | 000101-77-9 | Bis(4-aminophenyl)methane | 4A | SML = ND (DL = 0.01 mg/kg) |  |
| 13390 | 000105-08-8 | 1,4-Bis(hydroxymethyl)cyclohexane | 3 |  |  |
| 13395 | 004767-03-7 | 2,2-Bis(hydroxymethyl)propionic acid | 3 | QMA = 0.05 mg/6 dm² |  |
| 13480 | 000080-05-7 | 2,2-Bis(4-hydroxyphenyl)propane | 2 | SML = 0.6 mg/kg (28) | 0.01 |
| - | 039817-09-9 | Bis(hydroxyphenyl)methane bis(2,3-epoxypropyl) ether (= BFDGE, mixture of isomers) |  | SML = 0.05 mg/kg. For use only in the manufacture of heavy-duty coatings |  |
| 13510 | 001675-54-3 | 2,2-Bis(4-hydroxyphenyl)propane bis(2,3-epoxypropyl) ether (= BADGE) | 2-3 | According to Commission Regulation (EC) 1895/2005 of 18 November 2005 on the restriction of use of certain epoxy derivatives in materials and articles intended to come into contact with food | 0.15 |
| 13618 | 016068-37-4 | 1,2-Bis(triethoxysilyl)ethane | 3 | SML = 0.05 mg/kg when used for the surface treatment of materials |  |
| 13620 | 010043-35-3 | Boric acid | 2 | SML(T) = 6 mg/kg (23) (as B) without prejudice to the provi- sions of Directive 98/83/EC on water for human consump- tion | 0.1 (as B) |
| 13630 | 000106-99-0 | Butadiene | 4A | QM = 1 mg/kg in FP or SML = ND (DL = 0.020 mg/kg, analytical tolerance included) |  |
| 13690 | 000107-88-0 | 1,3-Butanediol | 1 |  | 4 |
| 13720 | 000110-63-4 | 1,4-Butanediol | 3 | SML(T) = 5 mg/kg (24) |  |
| 13780 | 002425-79-8 | 1,4-Butanediol bis(2,3-epoxypropyl) ether | 4A | QM = 1 mg/kg in FP (as epoxy group, Mw = 43) |  |
| 13810 | 000505-65-7 | 1,4-Butanediol formal | 3 | QMA = 0.05 mg/6 dm²) |  |
| 13845 | 000075-65-0 | tert-Butanol | 3 |  |  |
| 13870 | 000106-98-9 | 1-Butene | 3 |  |  |
| 13900 | 000107-01-7 | 2-Butene | 3 |  |  |
| 14020 | 000098-54-4 | 4-tert-Butylphenol | 3 | SML = 0.05 mg/kg |  |
| 14110 | 000123-72-8 | Butyraldehyde | 3 |  |  |
| (41760) | 008006-44-8 | Candelilla wax | 3 |  |  |
| 14200 | 000105-60-2 | Caprolactam | 2 | SML(T) = 15 mg/kg (5) | 0,25 |
| 14260 | 000502-44-3 | Caprolactone | 3 | SML = 0.05 mg/kg (as the sum of caprolactone and 6-hydroxyhexanoic acid) |  |
| 14320 | 000124-07-2 | Caprylic acid | 0 |  |  |
| (42160) | 000124-38-9 | Carbon dioxide | 1 |  | NS |
| 14380 | 000075-44-5 | Carbonyl chloride | 4A | QM = 1 mg/kg in FP |  |
| (42720) | 008015-86-9 | Carnauba wax | 3 |  |  |
| 14411 | 008001-79-4 | Castor oil | 3 |  |  |
| 14440 | 064147-40-6 | Castor oil, dehydrated | 3 |  |  |
| 14445 | 061789-44-4 | Castor oil fatty acids | 3 |  |  |
| 14450/1 | - | Castor oil fatty acids, dehydrated | 3 |  |  |
| 14453 | 061790-39-4 | Castor oil fatty acids, hydrogenated | 3 |  |  |
| 14470 | 008001-78-3 | Castor oil, hydrogenated | 3 |  |  |
| 14500 | 009004-34-6 | Cellulose | 0 |  |  |
| 14505 | 009004-35-7 | Cellulose acetate | 3 |  |  |
| 14508 | 009004-36-8 | Cellulose acetate butyrate | 3 |  |  |
| 14512 | 009004-39-1 | Cellulose acetate propionate | 3 |  |  |
| 14587 | 001204-28-0 | 4-(Chloroformyl)phthalic anhydride | 3 | QMA = 0.05 mg/6 dm² |  |
| 14650 | 000079-38-9 | Chlorotrifluoroethylene | 3 | QMA = 0.5 mg/6 dm² |  |
| 14680 | 000077-92-9 | Citric acid | 1 |  | NS |
| 14685 | 008001-31-8 | Coconut oil | 3 |  |  |
| 14693 | 008001-30-7 | Corn oil | 3 |  |  |
| 14695/1 | - | Corn oil fatty acids | 3 |  |  |
| 14698 | 008001-29-4 | Cottonseed oil | 3 |  |  |
| 14700/1 | - | Cottonseed oil fatty acids | 3 |  |  |
| 14710 | 000108-39-4 | m-Cresol | 3 |  |  |
| 14740 | 000095-48-7 | o-Cresol | 3 |  |  |
| 14770 | 000106-44-5 | p-Cresol | 3 |  |  |
| 14800 | 003724-65-0 | Crotonic acid | 3 | QMA(T) = 0.05 mg/6 dm² (33) |  |
| 14841 | 000599-64-4 | 4-Cumylphenol | 3 | SML = 0.05 mg/kg |  |
| 15095 | 000334-48-5 | n-Decanoic acid | 0 |  |  |
| 15310 | 000091-76-9 | 2,4-Diamino-6-phenyl-1,3,5-triazine | 3 | QMA = 5 mg/6 dm² |  |
| 15565 | 000106-46-7 | 1,4-Dichlorobenzene | 2 | SML = 12 mg/kg | 0.2 |
| 15610 | 000080-07-9 | 4,4'-Dichlorodiphenyl sulphone | 3 | SML = 0.05 mg/kg |  |
| 15695 | 000461-58-5 | Dicyanodiamide | 2 |  | 1 |
| 15700 | 005124-30-1 | Dicyclohexylmethane 4,4'-diisocyanate | 4A | QM(T) = 1 mg/kg (as NCO) (26) |  |
| 15760 | 000111-46-6 | Diethyleneglycol | 2 | SML(T) = 30 mg/kg (3) | 0,5 |
| 15790 | 000111-40-0 | Diethylenetriamine | 3 | SML = 5 mg/kg |  |
| 15880 | 000120-80-9 | 1,2-Dihydroxybenzene | 2 | SML = 6 mg/kg | 0,1 |
| 15910 | 000108-46-3 | 1,3-Dihydroxybenzene | 2 | SML = 2.4 mg/kg | 0,04 |
| 15940 | 000123-31-9 | 1,4-Dihydroxybenzene | 2 | SML = 0.6 mg/kg | 0,01 |
| 16090 | 000080-09-1 | 4,4'-Dihydroxydiphenyl sulphone | 3 | SML = 0.05 mg/kg |  |
| 16150 | 000108-01-0 | Dimethylaminoethanol | 2 | SML = 18 mg/kg | 0.3 |
| 16360 | 000576-26-1 | 2,6-Dimethylphenol | 3 | SML = 0.05 mg/kg |  |
| 16390 | 000126-30-7 | 2,2-Dimethyl-1,3-propanediol | 3 | SML = 0.05 mg/kg |  |
| 16480 | 000126-58-9 | Dipentaerythritol | 2 |  | 1 |
| 16600 | 005873-54-1 | Diphenylmethane 2,4'-diisocyanate | 4A | QM(T) = 1 mg/kg (as NCO) (26) |  |
| 16630 | 000101-68-8 | Diphenylmethane 4,4'-diisocyanate | 4A | QM(T) = 1 mg/kg (as NCO) (26) |  |
| 16660 | 000110-98-5 025265-71-8 | Dipropyleneglycol | 2 |  | 1,5 |
| 16690 | 001321-74-0 | Divinylbenzene | 4A | QMA = 0.01 mg/6 dm² or SML = ND (DL = 0.02 mg/kg, analytical tolerance included) for the sum of divinylbenzene and ethylvinylbenzene and in compliance with the specifica- tions laid down in Annex |  |
| 16697 | 000693-23-2 | n-Dodecanedioic acid | 3 |  |  |
| 16704 | 000112-41-4 | 1-Dodecene | 3 | SML = 0.05 mg/kg |  |
| 16750 | 000106-89-8 | Epichlorohydrin | 4A | QM = 1 mg/kg in FP |  |
| 16780 | 000064-17-5 | Ethanol | 1 |  |  |
| 16925 | 009004-57-3 | Ethylcellulose | 2 |  | NS |
| 16950 | 000074-85-1 | Ethylene | 3 |  |  |
| 16960 | 000107-15-3 | Ethylenediamine | 2 | SML = 12 mg/kg | 0,2 |
| 16990 | 000107-21-1 | Ethyleneglycol | 2 | SML(T) = 30 mg/kg (3) | 0,5 |
| 16993 | 000111-76-2 | Ethyleneglycol monobutyl ether | 2 | SML = 3 mg/kg | 0,05 |
| 16996 | 000110-80-5 | Ethyleneglycol monoethyl ether | 2 | SML = 3 mg/kg | 0,05 |
| 16999 | 000112-25-4 | Ethyleneglycol monohexyl ether | 2 | SML = 3 mg/kg | 0,05 |
| 17005 | 000151-56-4 | Ethyleneimine | 4A | SML = ND (DL = 0.01 mg/kg) |  |
| 17020 | 000075-21-8 | Ethylene oxide | 4A | QM = 1 mg/kg in FP |  |
| 17050 | 000104-76-7 | 2-Ethyl-1-hexanol | 1 | SML = 30 mg/kg | 0.5 |
| 17110 | 016219-75-3 | 5-Ethylidenebicyclo[2.2.1]hept-2-ene | 3 | QMA = 0.05 mg/6 dm². The ratio surface/quantity of food shall be lower than 2 dm²/kg |  |
| 17170 | 061788-47-4 | Fatty acids, coco | 3 |  |  |
| 17175 | 068938-15-8 | Fatty acids, coco, hydrogenated | 3 |  |  |
| 17200 | 068308-53-2 | Fatty acids, soya | 3 |  |  |
| 17215 | - | Fatty acids, sunflower oil | 3 |  |  |
| 17230 | 061790-12-3 | Fatty acids, tall oil | 3 |  |  |
| 17245 | 008016-13-5 | Fish oil | 3 |  |  |
| 17247/1 | - | Fish oil fatty acids | 3 |  |  |
| 17260 | 000050-00-0 | Formaldehyde | 3 | SML(T) = 15 mg/kg (22) |  |
| 17275 | 000064-18-6 | Formic acid | 1 |  | 3 |
| 17290 | 000110-17-8 | Fumaric acid | 1 |  | 6 |
| 18100 | 000056-81-5 | Glycerol | 1 |  | NS |
| 18115 | 031566-31-1 | Glycerol monostearate | 1 |  | NS |
| 18124 | 008016-24-8 | Hempseed oil | 3 |  |  |
| 18126/1 | - | Hempseed oil fatty acids | 3 |  |  |
| 18430 | 000116-15-4 | Hexafluoropropylene | 4A | SML = ND (DL = 0.01 mg/kg) |  |
| 18460 | 000124-09-4 | Hexamethylenediamine | 2 | SML = 2.4 mg/kg | 0,04 |
| 18640 | 000822-06-0 | Hexamethylene diisocyanate | 4A | QM(T) = 1 mg/kg (as NCO) (26) |  |
| 18670 | 000100-97-0 | Hexamethylenetetramine | 3 | SML(T) = 15 mg/kg (22) (as formaldehyde) |  |
| 18700 | 000629-11-8 | 1,6-Hexanediol | 3 | SML = 0.05 mg/kg |  |
| 18820 | 000592-41-6 | 1-Hexene | 3 | SML = 3 mg/kg |  |
| 18900 | 000106-14-9 | 12-Hydroxystearic acid | 0 |  |  |
| 19000 | 000115-11-7 | Isobutene | 3 |  |  |
| 19060 | 000109-53-5 | Isobutyl vinyl ether | 3 | QM = 5 mg/kg in FP |  |
| 19110 | 004098-71-9 | 1-Isocyanato-3-isocyanatomethyl-3,5,5-trimethylcyclohexane | 4A | QM(T) = 1 mg/kg (as NCO) (26) |  |
| 19112 | 103170-26-9 | 1-Isocyanato-3-isocyanatomethyl-3,5,5-trimethylcyclohexane homopolymer, methyl ethyl ketone oxime-blocked | 3 | SML = 0.05 mg/kg for the blocked trimer. Only to be used for thermoset coatings on light metal packaging. |  |
| 19150 | 000121-91-5 | Isophthalic acid | 3 | SML(T) = 5 mg/kg (43) |  |
| 19180 | 000099-63-8 | Isophthalic acid dichloride | 3 | SML(T) = 5 mg/kg (43) (expressed as isophthalic acid) |  |
| 19210 | 001459-93-4 | Isophthalic acid, dimethyl ester | 3 | SML = 0.05 mg/kg |  |
| 19270 | 000097-65-4 | Itaconic acid | 0 |  |  |
| 19460 | 000050-21-5 | Lactic acid | 1 |  | NS |
| 19470 | 000143-07-7 | Lauric acid | 0 |  |  |
| 19480 | 002146-71-6 | Lauric acid, vinyl ester | 3 |  |  |
| 19490 | 000947-04-6 | Laurolactam | 3 | SML = 5 mg/kg |  |
| 19518 | 000060-33-3 | Linoleic acid | 0 |  |  |
| 19526 | 028290-79-1 | Linolenic acid | 0 |  |  |
| 19532 | 008001-26-1 | Linseed oil | 3 |  |  |
| 19534/1 | - | Linseed oil fatty acids | 3 |  |  |
| 19540 | 000110-16-7 | Maleic acid | 2 | SML(T) = 30 mg/kg (4) | 0,5 |
| 19960 | 000108-31-6 | Maleic anhydride | 2 | SML(T) = 30 mg/kg (4) (as maleic acid) | 0,5 (as maleic acid) |
| (65020) | 006915-15-7 | Malic acid | 1 |  | NS |
| 19972 | 000087-78-5 | Mannitol | 1 |  |  |
| 19990 | 000079-39-0 | Methacrylamide | 4A | SML = ND (DL = 0.02 mg/kg, analytical tolerance included) |  |
| 20020 | 000079-41-4 | Methacrylic acid | 2 | SML(T) = 6 mg/kg (37) | 0,1 |
| 20050 | 000096-05-9 | Methacrylic acid, allyl ester | 3 | SML = 0.05 mg/kg |  |
| 20080 | 002495-37-6 | Methacrylic acid, benzyl ester | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 20110 | 000097-88-1 | Methacrylic acid, butyl ester | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 20140 | 002998-18-7 | Methacrylic acid, sec-butyl ester | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 20170 | 000585-07-9 | Methacrylic acid, tert-butyl ester | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 20260 | 000101-43-9 | Methacrylic acid, cyclohexyl ester | 3 | SML = 0.05 mg/kg |  |
| 20410 | 002082-81-7 | Methacrylic acid, diester with 1,4-butanediol | 3 | SML = 0.05 mg/kg |  |
| 20440 | 000097-90-5 | Methacrylic acid, diester with ethyleneglycol | 3 | SML = 0.05 mg/kg |  |
| 20530 | 002867-47-2 | Methacrylic acid, 2-(dimethylamino)ethyl ester | 4A | SML = ND (DL = 0.02 mg/kg, analytical tolerance included) |  |
| 20590 | 000106-91-2 | Methacrylic acid, 2,3-epoxypropyl ester | 4B | QMA = 0.02 mg/6 dm² |  |
| 20890 | 000097-63-2 | Methacrylic acid, ethyl ester | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 21010 | 000097-86-9 | Methacrylic acid, isobutyl ester | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 21100 | 004655-34-9 | Methacrylic acid, isopropyl ester | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 21130 | 000080-62-6 | Methacrylic acid, methyl ester | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 21190 | 000868-77-9 | Methacrylic acid, monoester with ethyleneglycol | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 21280 | 002177-70-0 | Methacrylic acid, phenyl ester | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 21340 | 002210-28-8 | Methacrylic acid, propyl ester | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 21370 | 010595-80-9 | Methacrylic acid, 2-sulphoethyl ester | 4A | QMA = ND (DL = 0.02 mg/6 dm²) |  |
| 21400 | 054276-35-6 | Methacrylic acid, sulphopropyl ester | 3 | QMA = 0.05 mg/6 dm² |  |
| 21460 | 000760-93-0 | Methacrylic anhydride | 2 | SML(T) = 6 mg/kg (37) (as methacrylic acid) | 0.1 (as m. acid) |
| 21490 | 000126-98-7 | Methacrylonitrile | 4A | SML = ND (DL = 0.02 mg/kg, analytical tolerance included) |  |
| 21520 | 001561-92-8 | Methallylsulphonic acid, sodium salt | 3 | SML = 5 mg/kg |  |
| 21550 | 000067-56-1 | Methanol | 3 |  |  |
| 21640 | 000078-79-5 | 2-Methyl-1,3-butadiene | 4A | QM = 1 mg/kg in FP or SML = ND (DL = 0.020 mg/kg, analytical tolerance included) |  |
| 21827 | 000078-93-3 | Methyl ethyl ketone | 3 | SML = 5 mg/kg |  |
| 21940 | 000924-42-5 | N-Methylolacrylamide | 4A | SML = ND (DL = 0.01 mg/kg) |  |
| 21970 | 000923-02-4 | N-Methylolmethacrylamide | 3 | SML = 0.05 mg/kg |  |
| 22190 | 002163-42-0 | 2-Methyl-1,3-propanediol | 3 | SML = 5 mg/kg |  |
| 22210 | 000098-83-9 | alpha-Methylstyrene | 3 | SML = 0.05 mg/kg |  |
| 22331 | 025513-64-8 | Mixture of (35-45% w/w) 1,6-diamino-2,2,4-trimethylhexane and (55-65% w/w) 1,6-diamino-2,4,4-trimethylhexane | 3 | QMA = 5 mg/6 dm² |  |
| 22333 | 000079-11-8 | Monochloroacetic acid | 3 | SML = 0.05 mg/kg |  |
| 22350 | 000544-63-8 | Myristic acid | 1 |  | NS |
| 22420 | 003173-72-6 | 1,5-Naphthalene diisocyanate | 4A | QM(T) = 1 mg/kg (as NCO) (26) |  |
| 22450 | 009004-70-0 | Nitrocellulose | 3 |  |  |
| 22660 | 000111-66-0 | 1-Octene | 2 | SML = 15 mg/kg | 0.25 |
| 22763 | 000112-80-1 | Oleic acid | 1 |  | NS |
| 22766 | 000143-28-2 | Oleyl alcohol | 3 |  |  |
| 22775 | 000144-62-7 | Oxalic acid | 2 | SML(T) = 6 mg/kg (29) | 0,1 |
| 22780 | 000057-10-3 | Palmitic acid | 1 |  | NS |
| 22840 | 000115-77-5 | Pentaerythritol | 2 |  | 1 |
| 22932 | 001187-93-5 | Perfluoromethyl perfluorovinyl ether | 3 | SML = 0.05 mg/kg. Only to be used for anti-stick coatings. |  |
| 22937 | 001623-05-8 | Perfluoropropyl perfluorovinyl ether | 3 | SML = 0.05 mg/kg |  |
| 22960 | 000108-95-2 | Phenol | 2 |  | 1,5 |
| 23050 | 000108-45-2 | 1,3-Phenylenediamine | 4A | SML = ND (DL = 0.02 mg/kg, analytical tolerance included) |  |
| 23170 | 007664-38-2 | Phosphoric acid | 1 |  | 70 (as P) |
| 23173 | 001314-56-3 | Phosphoric anhydride | 1 |  | 70 (as P) |
| 23200 | 000088-99-3 | o-Phthalic acid | 2 |  | 1 |
| 23230 | 000131-17-9 | Phthalic acid, diallyl ester | 4A | SML = ND (DL = 0.01 mg/kg) |  |
| 23380 | 000085-44-9 | Phthalic anhydride | 2 |  | 1 |
| 23470 | 000080-56-8 | alpha-Pinene | 3 |  |  |
| 23500 | 000127-91-3 | beta-Pinene | 3 |  |  |
| 23547 | 009016-00-6 063148-62-9 | Polydimethylsiloxane (MW > 6800) | 2 | In compliance with the speci- fications laid down in Annex |  |
| 23590 | 025322-68-3 | Polyethyleneglycol | 2 |  | 5 |
| 23651 | 025322-69-4 | Polypropyleneglycol | 3 |  |  |
| 23730 | 008002-11-7 | Poppyseed oil | 3 |  |  |
| 23740 | 000057-55-6 | 1,2-Propanediol | 1 |  | 25 |
| 23770 | 000504-63-2 | 1,3-Propanediol | 3 | SML = 0.05 mg/kg |  |
| 23800 | 000071-23-8 | 1-Propanol | 3 |  |  |
| 23830 | 000067-63-0 | 2-Propanol | 1 |  | 1,5 |
| 23860 | 000123-38-6 | Propionaldehyde | 3 |  |  |
| 23920 | 000105-38-4 | Propionic acid, vinyl ester | 2 | SML(T) = 6 mg/kg (2) (as acetaldehyde) | 0,1 |
| 23980 | 000115-07-1 | Propylene | 3 |  |  |
| 24010 | 000075-56-9 | Propylene oxide | 4A | QM = 1 mg/kg in FP |  |
| 24045 | 008016-49-7 | Pumpkinseed oil | 3 |  |  |
| 24055 | 000089-05-4 | Pyromellitic acid | 3 | SML = 0.05 mg/kg |  |
| 24057 | 000089-32-7 | Pyromellitic anhydride | 3 | SML = 0.05 mg/kg (as pyromellitic acid) |  |
| 24070 | 073138-82-6 | Resin acids and rosin acids | 2 |  | 1 |
| 24100 | 008050-09-7 | Rosin | 2 |  | 1 |
| 24115 | 008050-31-5 | Rosin, ester with glycerol | 1 |  | 12,5 |
| 24160 | 008052-10-6 | Rosin tall oil | 3 |  |  |
| 24250 | 009006-04-6 | Rubber, natural | 3 |  |  |
| 24260 | 008001-23-8 | Safflower oil | 3 |  |  |
| 24270 | 000069-72-7 | Salicylic acid | 3 |  |  |
| 24280 | 000111-20-6 | Sebacic acid | 2 |  | 3 |
| 24430 | 002561-88-8 | Sebacic anhydride | 2 |  |  |
| 24435 | 008008-74-0 | Sesame oil | 3 |  |  |
| 24440 | 009000-59-3 | Shellac | 1 |  |  |
| 24475 | 001313-82-2 | Sodium sulphide | 3 |  |  |
| 24490 | 000050-70-4 | Sorbitol | 1 |  |  |
| 24520 | 008001-22-7 | Soybean oil | 3 |  |  |
| (88880) | 068412-29-3 | Starch, hydrolysed | 0 |  |  |
| 24550 | 000057-11-4 | Stearic acid | 1 |  | NS |
| 24610 | 000100-42-5 | Styrene | 4B |  |  |
| 24760 | 026914-43-2 | Styrenesulphonic acid | 3 | SML = 0.05 mg/kg |  |
| 24820 | 000110-15-6 | Succinic acid | 1 |  | NS |
| 24850 | 000108-30-5 | Succinic anhydride | 2 |  | NS |
| 24880 | 000057-50-1 | Sucrose | 0 |  |  |
| 24887 | 006362-79-4 | 5-Sulphoisophthalic acid, monosodium salt | 3 | SML = 5 mg/kg |  |
| 24895 | 008001-21-6 | Sunflower oil | 3 |  |  |
| 24905 | 008002-26-4 | Tall oil | 3 |  |  |
| 24910 | 000100-21-0 | Terephthalic acid | 2 | SML = 7.5 mg/kg | 0,125 |
| 24940 | 000100-20-9 | Terephthalic acid dichloride | 2 | SML(T) = 7.5 mg/kg (as terephthalic acid) | 0,125 |
| 24970 | 000120-61-6 | Terephthalic acid, dimethyl ester | 2 |  | 1 |
| 25090 | 000112-60-7 | Tetraethyleneglycol | 1 |  | 10 |
| 25120 | 000116-14-3 | Tetrafluoroethylene | 3 | SML = 0.05 mg/kg |  |
| 25150 | 000109-99-9 | Tetrahydrofuran | 2 | SML = 0.6 mg/kg | 0,01 |
| 25208 | 026471-62-5 | Toluene diisocyanate | 4A | QM(T) = 1 mg/kg (as NCO) (26) |  |
| 25210 | 000584-84-9 | 2,4-Toluene diisocyanate | 4A | QM(T) = 1 mg/kg (as NCO) (26) |  |
| 25240 | 000091-08-7 | 2,6-Toluene diisocyanate | 4A | QM(T) = 1 mg/kg (as NCO) (26) |  |
| 25360 | - | Trialkyl(C5-C15)acetic acid, 2,3-epoxypropyl ester | 4A | QM = 1 mg/kg in FP (as epoxy group, Mw = 43) |  |
| 25380 | - | Trialkylacetic acid (C7-C17), vinyl esters (= Vinyl versatate) | 3 | QMA = 0.05 mg/6 dm² |  |
| 25420 | 000108-78-1 | 2,4,6-Triamino-1,3,5-triazine | 2 | SML = 30 mg/kg | 0,5 |
| 25450 | 026896-48-0 | Tricyclodecanedimethanol | 3 | SML = 0.05 mg/kg |  |
| 25510 | 000112-27-6 | Triethyleneglycol | 2 |  | 5 |
| 25540 | 000528-44-9 | Trimellitic acid | 3 | SML(T) = 5 mg/kg (35) |  |
| 25550 | 000552-30-7 | Trimellitic anhydride | 3 | SML(T) = 5 mg/kg (35) (as trimellitic acid) |  |
| 25573 | 016938-22-0 | 2,2,4-Trimethylhexane-1,6-diisocyanate | 4A | QM(T) = 1 mg/kg (as NCO) (26) |  |
| 25574 | 015646-96-5 | 2,4,4-Trimethylhexane-1,6-diisocyanate | 4A | QM(T) = 1 mg/kg (as NCO) (26) |  |
| 25600 | 000077-99-6 | 1,1,1-Trimethylolpropane | 2 | SML = 6 mg/kg | 0,1 |
| 25840 | 003290-92-4 | 1,1,1-Trimethylolpropane trimethacrylate | 3 | SML = 0.05 mg/kg |  |
| 25900 | 000110-88-3 | Trioxane | 3 | SML = 5 mg/kg |  |
| 25910 | 024800-44-0 | Tripropyleneglycol | 2 |  | 1,5 |
| 25960 | 000057-13-6 | Urea | 0 |  |  |
| 26050 | 000075-01-4 | Vinyl chloride | 4A | QM = 1 mg/kg in FP and SML = ND (DL = 0.01 mg/kg) |  |
| 26110 | 000075-35-4 | Vinylidene chloride | 4B | QM = 5 mg/kg in FP or SML = ND (DL = 0.05 mg/kg) |  |
| 26140 | 000075-38-7 | Vinylidene fluoride | 3 | SML = 5 mg/kg |  |
| 26155 | 001072-63-5 | 1-Vinylimidazole | 3 | QM = 5 mg/kg in FP |  |
| 26320 | 002768-02-7 | Vinyltrimethoxysilane | 3 | QM = 5 mg/kg in FP |  |
| 26340 | 008024-09-7 | Walnut oil | 3 |  |  |
| 26345/1 | - | Walnut oil fatty acids | 3 |  |  |
| 26360 | 007732-18-5 | Water | 0 | In compliance with Directive 98/83/EC |  |
| (95858) | - | Waxes, paraffinic, refined, derived from petroleum based or synthetic hydrocarbon feedstocks | 3 | SML = 0.05 mg/kg and in compliance with the specifications laid down in Annex. Not to be used for coatings contacting fatty foods. |  |
| (95859) | - | Waxes, refined, derived from petroleum based or synthetic hydrocarbon feedstocks | 2 | In compliance with the speci- fications laid down in Annex | 20 |
| 26370 | 001330-20-7 | Xylene | 3 | SML = 1.2 mg/kg | 0,02 |

B. TEMPORARY APPENDIX TO LIST 1 OF MONOMERS February 2009

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS |
| --- | --- | --- | --- | --- |
| (30350) | 000141-97-9 | Acetylacetic acid, ethyl ester | 7 | To be fixed |
| - | 068955-98-6 | Acids, fatty (C16-C18 and C18 unsaturated), branched and linear | - | To be fixed |
| 10720 | 000999-55-3 | Acrylic acid, allyl ester | 6A | To be fixed |
| 10930 | 003066-71-5 | Acrylic acid, cyclohexyl ester | 8 | To be fixed |
| 10990 | 002156-96-9 | Acrylic acid, decyl ester | 7 | To be fixed |
| 11050 | 001070-70-8 | Acrylic acid, diester with 1,4-butanediol | 8 | To be fixed |
| 11080 | 004074-88-8 | Acrylic acid, diester with diethyleneglycol | 8 | To be fixed |
| 11090 | 002223-82-7 | Acrylic acid, diester with 2,2-dimethyl-1,3-propanediol | 8 | To be fixed |
| 11110 | 002274-11-5 | Acrylic acid, diester with ethyleneglycol | 8 | To be fixed |
| 11140 | 013048-33-4 | Acrylic acid, diester with 1,6-hexanediol | 8 | To be fixed |
| 11170 | 026570-48-9 | Acrylic acid, diester with polyethyleneglycol | 8 | To be fixed |
| 11180 | 017831-71-9 | Acrylic acid, diester with tetraethyleneglycol | 8 | To be fixed |
| 11190 | 001680-21-3 | Acrylic acid, diester with triethyleneglycol | 8 | To be fixed |
| 11230 | 002439-35-2 | Acrylic acid, 2-(dimethylamino)ethyl ester | 7 | To be fixed |
| 11260 | 000106-90-1 | Acrylic acid, 2,3-epoxypropyl ester | 6A | To be fixed |
| 11425 | - | Acrylic acid, ester with methoxydiethyleneglycol | 8 | To be fixed |
| 11440 | 044992-01-0 | Acrylic acid, ester with trimethylethanolammonium chloride | 8 | To be fixed |
| - | 013402-02-3 | Acrylic acid, hexadecyl ester | - | To be fixed |
| 11620 | 001330-61-6 | Acrylic acid, isodecyl ester | 8 | To be fixed |
| 11650 | 029590-42-9 | Acrylic acid, isooctyl ester | 8 | To be fixed |
| 11695 | 003121-61-7 | Acrylic acid, 2-methoxyethyl ester | 6B | To be fixed |
| 11770 | 002478-10-6 | Acrylic acid, monoester with 1,4-butanediol | 8 | To be fixed |
| 11875 | 004813-57-4 | Acrylic acid, octadecyl ester | 7 | To be fixed |
| 12040 | 039121-78-3 | Acrylic acid, sulphopropyl ester | 8 | To be fixed |
| 12062 | 075577-70-7 | Acrylic acid, triester with 1,1,1-trimethylolpropane tris(2-hydroxyethyl) ether | 8 | To be fixed |
| 12070 | 002177-18-6 | Acrylic acid, vinyl ester | 7 | To be fixed |
| 12250 | 000123-79-5 | Adipic acid, di-n-octyl ester | 6B | To be fixed |
| - | 068855-58-3 | alpha-Alkenes (C10-C16) | - | To be fixed |
| 12573 | 068609-97-2 | Alkyl(C12-C14)-2,3-epoxypropyl ethers | 9 | To be fixed |
| 12650 | - | Allyl ethers of mono-, di-, or trimethylolphenol | 9 | To be fixed |
| 12772 | 000140-31-8 | N-Aminoethylpiperazine | 8 | To be fixed |
| 12775 | 000124-68-5 | 2-Amino-2-methyl-1-propanol | 8 | To be fixed |
| - | 009037-22-3 | Amylopectin | - | To be fixed |
| 13321 | 000080-04-6 | 2,2-Bis(4-hydroxycyclohexyl)propane | 8 | To be fixed |
| 13457 | 000620-92-8 | Bis(4-hydroxyphenyl)methane | 7 | To be fixed |
| 13465 | 000126-00-1 | 4,4-Bis(hydroxyphenyl)pentanoic acid | 8 | To be fixed |
| - | 025036-25-3 | 2,2-Bis(4-hydroxyphenyl)propane - 2,2-bis(4-hydroxyphenyl)propane bis(2,3-epoxy-propyl) ether, copolymer | - | To be fixed |
| - | 002778-42-9 | 1,3-Bis(alpha-isocyanatoisopropyl)benzene | - | To be fixed |
| 13915 | 000110-64-5 | 2-Buten-1,4-diol | 8 | To be fixed |
| 13960 | 001852-16-0 | N-(Butoxymethyl)acrylamide | 6A | To be fixed |
| 13990 | 005153-77-5 | N-(Butoxymethyl)methacrylamide | 6A | To be fixed |
| 14001 | 001320-16-7 | tert-Butylbenzoic acid | 8 | To be fixed |
| 14002 | 000098-73-7 | p-tert-Butylbenzoic acid | 7 | To be fixed |
| 14005 | 000098-29-3 | 4-tert-Butylcatechol | 8 | To be fixed |
| 14013 | 000115-84-4 | 2-Butyl-2-ethyl-1,3-propanediol | 8 | To be fixed |
| 14185 | 008015-80-3 | Candlenut oil | 8 | To be fixed |
| 14188/1 | - | Candlenut oil fatty acids | 8 | To be fixed |
| - | 008007-24-7 | Cashew nutshell oil | - | To be fixed |
| 14520 | 008001-20-5 | Chinawood oil | 8 | To be fixed |
| 14523/1 | - | Chinawood oil fatty acids | 8 | To be fixed |
| 14560 | 000126-99-8 | 2-Chloro-1,4-butadiene | 6A | To be fixed |
| 14836 | 014861-06-4 | Crotonic acid, vinyl ester | 7 | To be fixed |
| 14910 | 000108-94-1 | Cyclohexanone | 6A | To be fixed |
| 15735 | 000111-42-2 | Diethanolamine | 8 | To be fixed |
| 16100 | 060793-35-3 | 1,4-Dihydroxy-2-methylcyclohexane | 8 | To be fixed |
| 16115 | 025167-70-8 | Diisobutene | 8 | To be fixed |
| 16190 | 000121-69-7 | N,N-Dimethylaniline | 8 | To be fixed |
| 16200 | 000616-38-6 | Dimethyl carbonate | W8 | To be fixed |
| 16270 | 000526-75-0 | 2,3-Dimethylphenol | 8 | To be fixed |
| 16300 | 000105-67-9 | 2,4-Dimethylphenol | 8 | To be fixed |
| 16330 | 000095-87-4 | 2,5-Dimethylphenol | 8 | To be fixed |
| 16363 | 000095-65-8 | 3,4-Dimethylphenol | 8 | To be fixed |
| 16364 | 000108-68-9 | 3,5-Dimethylphenol | 8 | To be fixed |
| 16510 | 000138-86-3 | Dipentene | 8 | To be fixed |
| 16670 | 034590-94-8 | Dipropyleneglycol monomethyl ether | 8 | To be fixed |
| 16910 | 000111-35-3 | 3-Ethoxy-1-propanol | 8 | To be fixed |
| 17030 | 000094-96-2 | 2-Ethyl-1,3-hexanediol | 8 | To be fixed |
| 17040 | 000149-57-5 | 2-Ethylhexanoic acid | 6B | To be fixed |
| 17118 | 025429-37-2 | Ethylphenol | 8 | To be fixed |
| 17120 | 000090-00-6 | 2-Ethylphenol | 8 | To be fixed |
| 17121 | 000620-17-7 | 3-Ethylphenol | 8 | To be fixed |
| 17122 | 000123-07-9 | 4-Ethylphenol | 8 | To be fixed |
| 17150 | 000078-27-3 | 1-Ethynylcyclohexanol | 8 | To be fixed |
| - | 091051-35-3 | Fatty acids, peanut oil | - | To be fixed |
| 17233 | 073138-53-1 | Fatty acids, tall oil, dimers | 8 | To be fixed |
| 17350 | 000105-75-9 | Fumaric acid, dibutyl ester | 7 | To be fixed |
| 17500 | 000098-01-1 | Furfural | 7 | To be fixed |
| 17505 | 000098-00-0 | Furfurol | 8 | To be fixed |
| 18120 | 000107-22-2 | Glyoxal | 6A | To be fixed |
| 18441 | 000085-42-7 | Hexahydrophthalic anhydride | 8 | To be fixed |
| 18444 | 001076-97-7 | Hexahydroterephthalic acid | 7 | To be fixed |
| 18449 | 003089-11-0 | N,N,N',N',N",N"-Hexakis(methoxymethyl)-2,4,6-triamino-1,3,5-triazine | 8 | To be fixed |
| - | 000089-65-6 | Isoascorbic acid | - | To be fixed |
| 18970 | 000078-83-1 | Isobutanol | 8 | To be fixed |
| 19045 | 004548-27-0 | N-(Isobutoxymethyl)methacrylamide | 6A | To be fixed |
| 19240 | 000744-45-6 | Isophthalic acid, diphenyl ester | 8 | To be fixed |
| 19315 | 000617-52-7 | Itaconic acid, dimethyl ester | 8 | To be fixed |
| 19435 | - | Itaconic acid, methyl esters | 9 | To be fixed |
| - | 067746-08-1 | Linseed oil, polymerised | - | To be fixed |
| 19570 | 000999-21-3 | Maleic acid, diallyl ester | 6A | To be fixed |
| 19600 | 000105-76-0 | Maleic acid, dibutyl ester | 7 | To be fixed |
| 19750 | 000624-48-6 | Maleic acid, dimethyl ester | 7 | To be fixed |
| 19780 | 002915-53-9 | Maleic acid, dioctyl ester | 7 | To be fixed |
| 19900 | 002424-58-0 | Maleic acid, monoallyl ester | 6A | To be fixed |
| 19936 | 007423-42-9 | Maleic acid, mono(2-ethylhexyl) ester | 8 | To be fixed |
| 19945 | 003052-50-4 | Maleic acid, monomethyl ester | 7 | To be fixed |
| 19977 | 000060-24-2 | 2-Mercaptoethanol | 8 | To be fixed |
| 20005 | 051410-72-1 | Methacrylamidopropyltrimethylammonium chloride | 6A | To be fixed |
| - | 090551-76-1 | Methacrylic acid, alkyl(C12-C16) esters | - | To be fixed |
| - | 090551-83-0 | Methacrylic acid, alkyl(C16-C18) esters | - | To be fixed |
| - | 003775-90-4 | Methacrylic acid, 2-(tert-butylamino)ethyl ester | - | To be fixed |
| 20320 | 003179-47-3 | Methacrylic acid, decyl ester | 7 | To be fixed |
| 20380 | 001189-08-8 | Methacrylic acid, diester with 1,3-butanediol | 8 | To be fixed |
| 20425 | 002358-84-1 | Methacrylic acid, diester with diethyleneglycol | 8 | To be fixed |
| 20430 | 001985-51-9 | Methacrylic acid, diester with 2,2-dimethyl-1,3-propanediol | 8 | To be fixed |
| 20455 | 006606-59-3 | Methacrylic acid, diester with 1,6-hexanediol | 8 | To be fixed |
| 20490 | 000109-17-1 | Methacrylic acid, diester with tetraethyleneglycol | 8 | To be fixed |
| - | 000109-16-0 | Methacrylic acid, diester with triethyleneglycol | - | To be fixed |
| 20560 | 000142-90-5 | Methacrylic acid, dodecyl ester | 7 | To be fixed |
| 20740 | 039670-09-2 | Methacrylic acid, ester with ethoxytriethyleneglycol | 8 | To be fixed |
| 20830 | - | Methacrylic acid, esters with 1,2-propanediol | 8 | To be fixed |
| 20860 | 005039-78-1 | Methacrylic acid, ester with trimethylethanolammonium chloride | 8 | To be fixed |
| 20875 | 002370-63-0 | Methacrylic acid, 2-ethoxyethyl ester | 8 | To be fixed |
| 20920 | 000688-84-6 | Methacrylic acid, 2-ethylhexyl ester | 8 | To be fixed |
| 20935 | 002495-27-4 | Methacrylic acid, hexadecyl ester | 7 | To be fixed |
| 20940 | 000142-09-6 | Methacrylic acid, hexyl ester | 7 | To be fixed |
| 20945 | 004664-49-7 | Methacrylic acid, 2-hydroxyisopropyl ester | 7 | To be fixed |
| 20950 | 000923-26-2 | Methacrylic acid, 2-hydroxypropyl ester | 8 | To be fixed |
| 20980 | 007534-94-3 | Methacrylic acid, isobornyl ester | 8 | To be fixed |
| 21040 | 029964-84-9 | Methacrylic acid, isodecyl ester | 8 | To be fixed |
| 21220 | 032360-05-7 | Methacrylic acid, octadecyl ester | 8 | To be fixed |
| 21250 | 002157-01-9 | Methacrylic acid, n-octyl ester | 7 | To be fixed |
| 21415 | 002549-53-3 | Methacrylic acid, tetradecyl ester | 7 | To be fixed |
| - | 007779-31-9 | Methacrylic acid, 3,3,5-trimethylcyclohexyl ester | - | To be fixed |
| 21430 | 004245-37-8 | Methacrylic acid, vinyl ester | 7 | To be fixed |
| - | 004203-89-8 | 3-[2-(Methacryloxy)ethyl]-2,2-spirocyclohexyloxazolidine | - | To be fixed |
| 21580 | 003644-11-9 | N-(Methoxymethyl)acrylamide | 6A | To be fixed |
| 21610 | 003644-12-0 | N-(Methoxymethyl)methacrylamide | 6A | To be fixed |
| 21615 | 000150-76-5 | 4-Methoxyphenol | 8 | To be fixed |
| 21620 | 000107-98-2 | 1-Methoxy-2-propanol | 8 | To be fixed |
| 21630 | 001187-59-3 | N-Methylacrylamide | 6A | To be fixed |
| 21733 | 000115-19-5 | 2-Methyl-3-butyn-2-ol | 8 | To be fixed |
| 21790 | 000110-26-9 | Methylenebisacrylamide | 6A | To be fixed |
| 22240 | 000622-97-9 | p-Methylstyrene | 6A | To be fixed |
| 22510 | 027215-95-8 | Nonene | 8 | To be fixed |
| 22535 | 025154-52-3 | Nonylphenol | 9 | To be fixed |
| 22540 | 000104-40-5 | 4-Nonylphenol | 8 | To be fixed |
| 22690 | 001806-26-4 | 4-Octylphenol | 8 | To be fixed |
| 22755 | 008016-35-1 | Oiticica oil | 8 | To be fixed |
| 22757/1 | - | Oiticica oil fatty acids | 8 | To be fixed |
| 22800 | 000501-24-6 | 3-Pentadecylphenol | 8 | To be fixed |
| 23140 | 000092-69-3 | 4-Phenylphenol | 8 | To be fixed |
| - | 157567-90-3 | Polyethyleneglycol isotridecyl ether methacrylate | - | To be fixed |
| 23680 | 009002-89-5 | Polyvinyl alcohols | 7 | To be fixed |
| 23710 | 063148-65-2 | Polyvinylbutyrals | 9 | To be fixed |
| 24150 | 065997-05-9 | Rosin, polymerised | 9 | To be fixed |
| 24525 | - | Soybean oil fatty acids, dimers | 8 | To be fixed |
| 24560 | 000111-63-7 | Stearic acid, vinyl ester | 8 | To be fixed |
| 24835 | 000106-65-0 | Succinic acid, dimethyl ester | 7 | To be fixed |
| 24900 | - | Sunflower oil fatty acids, dimers | D | To be fixed |
| - | 005593-70-4 | Tetrabutyl titanate | - | To be fixed |
| 25105 | 000112-57-2 | Tetraethylenepentamine | 8 | To be fixed |
| 25161 | 000085-43-8 | 1,2,3,6-Tetrahydrophthalic anhydride | 8 | To be fixed |
| 25163 | 002426-02-0 | 3,4,5,6-Tetrahydrophthalic anhydride | 8 | To be fixed |
| - | 006334-25-4 | N,N,N',N'-Tetrakis(2-hydroxyethyl)hexanediamide | - | To be fixed |
| 25185 | 000140-66-9 | 4-(1,1,3,3-Tetramethylbutyl)phenol | 6B | To be fixed |
| 25191 | 000126-86-3 | 2,4,7,9-Tetramethyl-5-decyne-4,7-diol | 8 | To be fixed |
| 25300 | 000088-19-7 | o-Toluenesulphonamide | 8 | To be fixed |
| 25330 | 000070-55-3 | p-Toluenesulphonamide | 7 | To be fixed |
| 25390 | 000101-37-1 | Triallyl cyanurate | 6A | To be fixed |
| 25405 | 001025-15-6 | Triallyl isocyanurate | 6A | To be fixed |
| 25480 | 000102-71-6 | Triethanolamine | 8 | To be fixed |
| 25520 | 000112-24-3 | Triethylenetetramine | 8 | To be fixed |
| 25595 | 000077-85-0 | Trimethylolethane | 9 | To be fixed |
| 25660 | 019727-16-3 | 1,1,1-Trimethylolpropane dimethacrylate | 7 | To be fixed |
| 25810 | 015625-89-5 | 1,1,1-Trimethylolpropane triacrylate | 8 | To be fixed |
| 25855 | 000144-19-4 | 2,2,4-Trimethyl-1,3-pentanediol | 8 | To be fixed |
| 25915 | 000090-72-2 | 2,4,6-Tris[(dimethylamino)methyl]phenol | 8 | To be fixed |
| 26260 | 001184-84-5 | Vinylsulphonic acid | 6A | To be fixed |
| - | 003039-83-6 | Vinylsulphonic acid, sodium salt | - | To be fixed |
| 26290 | 025013-15-4 | Vinyltoluene | 7 | To be fixed |

C. LIST 1 OF ADDITIVES February 2009

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| --- | --- | --- | --- | --- | --- |
| 30000 | 000064-19-7 | Acetic acid | 1 |  | NS |
| 30045 | 000123-86-4 | Acetic acid, butyl ester | 1 |  | 6 |
| 30140 | 000141-78-6 | Acetic acid, ethyl ester | 1 |  | NS |
| 30295 | 000067-64-1 | Acetone | 3 |  |  |
| 30401 | - | Acetylated mono- and diglycerides of fatty acids | 1 |  | NS |
| 30610 | - | Acids, C2-C24, aliphatic, linear, monocarboxylic, from natural oils and fats and their mono-, di- and triglycerol esters (branched fatty acids at naturally occuring levels are included) | 3 |  |  |
| 30612 | - | Acids, C2-C24, aliphatic, linear, monocarboxylic, synthetic, and their mono-, di- and triglycerol esters | 3 |  |  |
| 30960 | - | Acids, aliphatic, monocarboxylic (C6-C22), esters with polyglycerol | 1 |  | 25 |
| 31328 | - | Acids, fatty, from animal or vegetable food fats and oils | 3 |  |  |
| 31520 | 061167-58-6 | Acrylic acid, 2-tert-butyl-6-(3-tert-butyl-2-hydroxy-5-methylbenzyl)-4-methylphenyl ester | 2 | SML = 6 mg/kg | 0,1 |
| 31542 | 174254-23-0 | Acrylic acid, methyl ester, telomer with 1-dodecanethiol, C16-C18 alkyl esters | 3 | QM = 0.5 % in FP |  |
| 31730 | 000124-04-9 | Adipic acid | 1 |  | 5 |
| 31920 | 000103-23-1 | Adipic acid, bis(2-ethylhexyl) ester | 2 | SML = 18 mg/kg (1) | 0.3 |
| 33120 | - | Alcohols, aliphatic, monohydric, saturated, linear, primary (C4-C24) | 3 |  |  |
| 33801 | - | n-Alkyl(C10-C13)benzenesulphonic acid | 2 | SML = 30 mg/kg | 0.5 |
| 34230 | - | Alkyl(C8-C22)sulphonic acids | 2 | SML = 6 mg/kg | 0.1 |
| 34281 | - | Alkyl(C8-C22)sulphuric acids, linear, primary, with an even number of carbon atoms | 3 |  |  |
| 34480 | - | Aluminium fibers, flakes and powders | 2 |  | 1 (as Al) |
| 34560 | 021645-51-2 | Aluminium hydroxide | 2 |  | 1 (as Al) |
| 34720 | 001344-28-1 | Aluminium oxide | 2 |  | 1 (as Al) |

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| --- | --- | --- | --- | --- | --- |
| 35170 | 000141-43-5 | 2-Aminoethanol | 3 | SML = 0.05 mg/kg. Not for use in polymers contacting foods for which simulant D is laid down in Directive 85/572/EEC and for indirect food contact only, behind the PET layer. |  |
| 35284 | 000111-41-1 | N-(2-Aminoethyl)ethanolamine | 3 | SML = 0.05 mg/kg. Not for use in polymers contacting foods for which simulant D is laid down in Directive 85/572/EEC and for indirect food contact only, behind the PET layer. |  |
| 35320 | 007664-41-7 | Ammonia | 1 |  | NS |
| 35520 | 012125-02-9 | Ammonium chloride | 1 |  | NS |
| 35600 | 001336-21-6 | Ammonium hydroxide | 1 |  | NS |
| 35760 | 001309-64-4 | Antimony trioxide | 3 | SML = 0.04 mg/kg (39) (as Sb) |  |
| 36000 | 000050-81-7 | Ascorbic acid | 1 |  |  |
| 36720 | 017194-00-2 | Barium hydroxide | 3 | SML(T) = 1 mg/kg (12) (as Ba) |  |
| 36880 | 008012-89-3 | Beeswax | 0 |  |  |
| 37040 | 000112-85-6 | Behenic acid | 0 |  |  |
| 37280 | 001302-78-9 | Bentonite | 3 |  |  |
| 37520 | 002634-33-5 | 1,2-Benzisothiazolin-3-one | 3 | SML = 0.5 mg/kg. Only to be used in aqueous polymer dispersions and emulsions and at concentrations which do not result in an antimicrobial effect at the surface of the polymer or on the food itself. |  |
| 37600 | 000065-85-0 | Benzoic acid | 1 |  | 5 |
| 38000 | 000553-54-8 | Benzoic acid, lithium salt | 1-2 | SML(T) = 0.6 mg/kg (8) (as Li) | 0.01 (Li) |
| 38240 | 000119-61-9 | Benzophenone | 2 | SML = 0.6 mg/kg | 0.01 |
| 38515 | 001533-45-5 | 4,4'-Bis(2-benzoxazolyl)stilbene | 3 | SML = 0.05 mg/kg (1) |  |
| 38560 | 007128-64-5 | 2,5-Bis(5-tert-butyl-2-benzoxazolyl)thiophene | 2 | SML = 0.6 mg/kg | 0.01 |
| 38800 | 032687-78-8 | N,N'-Bis[3-(3,5-di-tert-butyl-4-hydroxyphenyl)propionyl]hydrazide | 2 | SML = 15 mg/kg | 0.25 |
| 38885 | 002725-22-6 | 2,4-Bis(2,4-dimethylphenyl)-6-(2-hydroxy-4-n-octyloxyphenyl)-1,3,5-triazine | 3 | SML = 0.05 mg/kg For aqueous foods only. |  |
| 39090 | - | N,N-Bis(2-hydroxyethyl)alkyl(C8-C18)amine | 2 | SML(T) = 1.2 mg/kg (13) | 0.02 (free a.) |
| 39200 | 006200-40-4 | Bis(2-hydroxyethyl)-2-hydroxypropyl-3-(dodecyloxy)-methylammonium chloride | 2 | SML = 1.8 mg/kg | 0.03 |

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| --- | --- | --- | --- | --- | --- |
| 39700 | 001675-54-3 | 2,2-Bis(4-hydroxyphenyl)propane bis(2,3-epoxypropyl) ether (= BADGE) | 2-3 | According to Commission Regulation (EC) 1895/2005 of 18 November 2005 on the restriction of use of certain epoxy derivatives in materials and articles intended to come into contact with food. | 0.15 |
| 39890 | 087826-41-3 069158-41-4 054686-97-4 081541-12-0 | Bis(methylbenzylidene)sorbitol | 2 |  | 1 |
| 40000 | 000991-84-4 | 2,4-Bis(octylmercapto)-6-(4-hydroxy-3,5-di-tert-butylanilino)-1,3,5-triazine | 2 | SML = 30 mg/kg | 0.5 |
| 40020 | 110553-27-0 | 2,4-Bis(octylthiomethyl)-6-methylphenol | 2 | SML(T) = 5 mg/kg (40) |  |
| 40120 | 068951-50-8 | Bis(polyethyleneglycol) hydroxymethylphosphonate | 3 | SML = 0.6 mg/kg |  |
| 40320 | 010043-35-3 | Boric acid | 2 | SML(T) = 6 mg/kg (23) (as B) without prejudice to the provisions of Directive 98/83/EC on water for human consumption |  |
| 40580 | 000110-63-4 | 1,4-Butanediol | 3 | SML(T) = 5 mg/kg (24) |  |
| 40590 | 000071-36-3 | 1-Butanol | 3 |  |  |
| 40594 | 000075-65-0 | tert-Butanol | 3 |  |  |
| 40800 | 013003-12-8 | 4,4'-Butylidenebis(6-tert-butyl-3-methylphenyl-ditridecyl phosphite) | 2 | SML = 6 mg/kg | 0.1 |
| 41120 | 010043-52-4 | Calcium chloride | 1 |  | NS |
| 41280 | 001305-62-0 | Calcium hydroxide | 1 |  | NS |
| 41520 | 001305-78-8 | Calcium oxide | 1 |  | NS |
| 41760 | 008006-44-8 | Candelilla wax | 3 |  |  |
| 41960 | 000124-07-2 | Caprylic acid | 0 |  |  |
| 42080 | 001333-86-4 | Carbon black | 3 | In compliance with the specifications laid down in Annex |  |
| 42160 | 000124-38-9 | Carbon dioxide | 1 |  | NS |
| 42500 | - | Carbonic acid, salts | 1 |  | NS (CO3) |
| 42640 | 009000-11-7 | Carboxymethylcellulose | 2 |  | NS |
| 42720 | 008015-86-9 | Carnauba wax | 3 |  |  |
| 42800 | 009000-71-9 | Casein | 0 |  |  |
| 42880 | 008001-79-4 | Castor oil | 3 |  |  |
| 43120 | 008001-78-3 | Castor oil, hydrogenated | 3 |  |  |
| 43200 | - | Castor oil, mono- and diglycerides | 3 |  |  |
| 43280 | 009004-34-6 | Cellulose | 0 |  |  |
| 43300 | 009004-36-8 | Cellulose acetate butyrate | 3 |  |  |
| 43515 | - | Chlorides of choline esters of coconut oil fatty acids | 3 | QMA = 0.9 mg/6 dm² |  |
| 44160 | 000077-92-9 | Citric acid | 1 |  | NS |
| 44640 | 000077-93-0 | Citric acid, triethyl ester | 1 |  | 20 |
| 45450 | 068610-51-5 | p-Cresol-dicyclopentadiene-isobutylene, copolymer | 3 | SML = 5 mg/kg |  |
| 45560 | 014464-46-1 | Cristobalite | 3 |  |  |
| 45940 | 000334-48-5 | n-Decanoic acid | 0 |  |  |
| - | 009004-53-9 | Dextrin | - | In compliance with the FCC specifications |  |
| 46070 | 010016-20-3 | alpha-Dextrin | 0 |  |  |
| 46080 | 007585-39-9 | beta-Dextrin | 0 |  |  |
| 46380 | 068855-54-9 | Diatomaceous earth, soda ash flux-calcined | 3 |  |  |
| 46480 | 032647-67-9 | Dibenzylidene sorbitol | 2 |  | 1 |
| 46640 | 000128-37-0 | 2,6-Di-tert-butyl-p-cresol (= BHT) | 1 | SML = 3 mg/kg | 0,05 |
| 46790 | 004221-80-1 | 3,5-Di-tert-butyl-4-hydroxybenzoic acid, 2,4-di-tert-butylphenyl ester | 2 |  | 2 |
| 46800 | 067845-93-6 | 3,5-Di-tert-butyl-4-hydroxybenzoic acid, hexadecyl ester | 2 |  | 2.5 |
| 46880 | 065140-91-2 | 3,5-Di-tert-butyl-4-hydroxybenzylphosphonic acid, monoethyl ester, calcium salt | 2 | SML = 6 mg/kg | 0.1 |
| 47440 | 000461-58-5 | Dicyanodiamide | 2 |  | 1 |
| 47520 | - | Dicyclopentadiene-indene-styrene-alpha-methylstyrene-vinyltoluene-isobutylene, copolymer, hydrogenated | 3 | SML = 5 mg/kg |  |
| 48030 | 000112-34-5 | Diethyleneglycol monobutyl ether | 2 | SML = 3 mg/kg | 0.5 |
| 49235 | 000108-01-0 | Dimethylaminoethanol | 2 | SML = 18 mg/kg | 0,3 |
| 49485 | 134701-20-5 | 2,4-Dimethyl-6-(1-methylpentadecyl)phenol | 3 | SML = 1 mg/kg |  |
| 49840 | 002500-88-1 | Dioctadecyl disulphide | 2 | SML = 3 mg/kg | 0,05 |
| 50320 | 015571-58-1 | Di-n-octyltin bis(2-ethylhexyl mercaptoacetate) | 2 | SML(T) = 0.006 mg/kg (17) (as Sn) | ? |
| 50640 | 003648-18-8 | Di-n-octyltin dilaurate | 2 | SML(T) = 0.006 mg/kg (17) (as Sn) | ? |
| 51760 | 025265-71-8 000110-98-5 | Dipropyleneglycol | 2 |  | 1,5 |
| - | 055963-33-2 | Distarch phosphate | - | In compliance with the specifications of food additive E1412 | ACC |
| - | 068130-14-3 | Distarch phosphate acetate | - | In compliance with the specifications of food additive E1414 | ACC |
| 52000 | 027176-87-0 | Dodecylbenzenesulphonic acid | 2 | SML = 30 mg/kg | 0,5 |
| 52640 | 016389-88-1 | Dolomite | 3 |  |  |
| 52720 | 000112-84-5 | Erucamide | 3 |  |  |
| 52730 | 000112-86-7 | Erucic acid | 3 |  |  |
| 52800 | 000064-17-5 | Ethanol | 1 |  |  |
| 53200 | 023949-66-8 | 2-Ethoxy-2'-ethyloxanilide | 2 | SML = 30 mg/kg | 0,5 |
| 53255 | 000100-41-4 | Ethylbenzene | 3 | To be fixed |  |
| 53280 | 009004-57-3 | Ethylcellulose | 2 |  | NS |
| 53360 | 000110-31-6 | N,N'-Ethylenebisoleamide | 3 |  |  |
| 53440 | 005518-18-3 | N,N'-Ethylenebispalmitamide | 3 |  |  |
| 53520 | 000110-30-5 | N,N'-Ethylenebisstearamide | 3 |  |  |
| 53540 | 000107-15-3 | Ethylenediamine | 2 | SML = 12 mg/kg | 0,2 |
| 53600 | 000060-00-4 | Ethylenediaminetetraacetic acid | 2 |  | 2,5 |
| 53650 | 000107-21-1 | Ethyleneglycol | 2 | SML(T) = 30 mg/kg (3) | 0,5 |
| 53670 | 032509-66-3 | Ethyleneglycol bis[3,3-bis(3-tert-butyl-4-hydroxyphenyl)butyrate] | 2 | SML = 6 mg/kg | 0,1 |
| 53820 | 000110-80-5 | Ethyleneglycol monoethyl ether | 2 | SML = 3 mg/kg | 0,05 |
| 54450 | - | Fats and oils, from animal or vegetable food sources | 3 |  |  |
| 54480 | - | Fats and oils, hydrogenated, from animal or vegetable food sources | 3 |  |  |
| 54710/1 | 061790-12-3 | Fatty acids, tall oil | 3 |  |  |
| 54730/1 | - | Fatty acids, tall oil, cobalt salts | 3 | SML(T) = 0.05 mg/kg (14) (as Co) |  |
| 54880 | 000050-00-0 | Formaldehyde | 3 | SML(T) = 15 mg/kg (22) |  |
| 55040 | 000064-18-6 | Formic acid | 1 |  | 3 |
| - | 000526-95-4 | Gluconic acid | - | In compliance with the specifications of food additive E574 | NS |
| 55910 | 736150-63-3 | Glycerides, castor-oil mono-, hydrogenated, acetates | ? |  |  |
| 56000 | 025395-31-7 | Glycerol diacetate | 1 |  | NS |
| 56080 | 025637-84-7 | Glycerol dioleate | 1 |  | NS |
| 56320 | 001323-83-7 | Glycerol distearate | 1 |  | NS |
| 56486 | - | Glycerol, esters with acids, aliphatic, saturated, linear, with an even number of carbon atoms (C14-C18) and with acids, aliphatic, unsaturated, linear, with an even number of carbon atoms (C16-C18) | 3 |  |  |
| 56500 | - | Glycerol, esters with lauric acid | 3 |  |  |
| 56580 | - | Glycerol, esters with ricinoleic acid | 3 |  |  |
| 56610 | 030233-64-8 | Glycerol monobehenate | 3 |  |  |
| 56800 | 030899-62-8 | Glycerol monolaurate diacetate | 3 |  |  |
| 56960 | 025496-72-4 | Glycerol monooleate | 1 |  | NS |
| 57520 | 031566-31-1 | Glycerol monostearate | 1 |  | NS |
| 57760 | 000102-76-1 | Glycerol triacetate | 1 |  | NS |
| 58480 | 009000-01-5 | Gum arabic | 1 |  | NS |
| 59120 | 023128-74-7 | 1,6-Hexamethylenebis[3-(3,5-di-tert-butyl-4-hydroxyphenyl)propionamide] | 2 | SML = 45 mg/kg | 0,75 |
| 59200 | 035074-77-2 | 1,6-Hexamethylenebis[3-(3,5-di-tert-butyl-4-hydroxyphenyl)propionate] | 2 | SML = 6 mg/kg | 0.1 |
| 59240 | 000124-09-4 | Hexamethylenediamine | 2 | SML = 2.4 mg/kg | 0,04 |
| 59280 | 000100-97-0 | Hexamethylenetetramine | 3 | SML(T) = 15 mg/kg (22) (as formaldehyde) |  |
| 59990 | 007647-01-0 | Hydrochloric acid | 1 |  | NS |
| 60200 | 000099-76-3 | 4-Hydroxybenzoic acid, methyl ester | 1 |  | 10 |
| 60320 | 070321-86-7 | 2-[2-Hydroxy-3,5-bis(1,1-dimethylbenzyl)phenyl]benzotriazole | 2 | SML = 1.5 mg/kg | 0.025 |
| 60400 | 003896-11-5 | 2-(2'-Hydroxy-3'-tert-butyl-5'-methylphenyl)-5-chlorobenzotriazole | 2 | SML(T) = 30 mg/kg (19) | 0,5 |
| 60480 | 003864-99-1 | 2-(2'-Hydroxy-3,5-di-tert-butylphenyl)-5-chlorobenzotriazole | 2 | SML(T) = 30 mg/kg (19) | 0,5 |
| 60560 | 009004-62-0 | Hydroxyethylcellulose | 2 |  | NS |
| 60800 | 065447-77-0 | 1-(2-Hydroxyethyl)-4-hydroxy-2,2,6,6-tetramethylpiperidine - succinic acid, dimethyl ester, copolymer | 2 | SML = 30 mg/kg | 0.5 |
| 60880 | 009032-42-2 | Hydroxyethylmethylcellulose | 2 |  | NS |
| 61360 | 000131-57-7 | 2-Hydroxy-4-methoxybenzophenone | 2 | SML(T) = 6 mg/kg (15) | 0,1 |
| 61440 | 002440-22-4 | 2-(2'-Hydroxy-5'-methylphenyl)benzotriazole | 2 | SML(T) = 30 mg/kg (19) | 0,5 |
| 61600 | 001843-05-6 | 2-Hydroxy-4-n-octyloxybenzophenone | 2 | SML(T) = 6 mg/kg (15) | 0,1 |
| 61680 | 009004-64-2 | Hydroxypropylcellulose | 2 |  | NS |
| 61800 | 009049-76-7 | Hydroxypropyl starch | 1 |  | NS |
| 61840 | 000106-14-9 | 12-Hydroxystearic acid | 0 |  |  |
| 62140 | 006303-21-5 | Hypophosphorous acid | 3 |  |  |
| 62220 | 010045-89-3 | Iron(II) diammonium bisulphate | 3 |  |  |
| 62240 | 001332-37-2 | Iron oxide | 2 |  | NS |
| 62640 | 008001-39-6 | Japan wax | 3 |  |  |
| 62720 | 001332-58-7 | Kaolin | 1 |  | NS |
| 62800 | - | Kaolin, calcined | 3 |  |  |
| 62960 | 000050-21-5 | Lactic acid | 1 |  | NS |
| 63040 | 000138-22-7 | Lactic acid, butyl ester | 2 |  | NS |
| 63240 | 008006-54-0 | Lanolin | 0 |  |  |
| 63280 | 000143-07-7 | Lauric acid | 0 |  |  |
| 63760 | 008002-43-5 | Lecithin | 1 |  | NS |
| 63940 | 008062-15-5 | Lignosulphonic acid | 3 | SML = 0.24 mg/kg. To be used only as dispersant for plastics dispersions |  |
| 64015 | 000060-33-3 | Linoleic acid | 0 |  |  |
| 64150 | 028290-79-1 | Linolenic acid | 0 |  |  |
| 64160 | 008001-26-1 | Linseed oil | 3 |  |  |
| 64300 | 001310-65-2 | Lithium hydroxide | 2 | SML(T) = 0.6 mg/kg (8) (as Li) | 0.01 (Li) |
| 64400 | 001345-05-7 | Lithopone | 3 |  |  |
| 64560 | 007786-30-3 | Magnesium chloride | 1 |  | NS |
| 64720 | 001309-48-4 | Magnesium oxide | 1 |  | NS |
| 65020 | 006915-15-7 | Malic acid | 1 |  | NS |
| 65960 | 000067-56-1 | Methanol | 3 |  |  |
| 66200 | 037206-01-2 | Methylcarboxymethylcellulose | 2 |  | NS |
| 66240 | 009004-67-5 | Methylcellulose | 2 |  | NS |
| 66400 | 000088-24-4 | 2,2'-Methylenebis(4-ethyl-6-tert-butylphenol) | 2 | SML(T) = 1.5 mg/kg (20) | 0.025 |
| 66480 | 000119-47-1 | 2,2'-Methylenebis(4-methyl-6-tert-butylphenol) | 2 | SML(T) = 1.5 mg/kg (20) | 0.025 |
| 66700 | 009004-65-3 | Methylhydroxypropylcellulose | 2 |  | NS |
| 66755 | 002682-20-4 | 2-Methyl-4-isothiazolin-3-one | 3 | SML = 0.5 mg/kg. Only to be used in aqueous polymer dispersions and emulsions and at concentrations which do not result in an anti-microbial effect at the surface of the polymer or on the food itself. |  |
| 66905 | 000872-50-4 | N-Methylpyrrolidone | 2 |  | ? |
| 66930 | 068554-70-1 | Methylsilsesquioxane | 3 | Residual monomer in methyl-silsesquioxane < 1 mg methyltrimethoxysilane/kg of methyl-silsequioxane |  |
| 66950 | 068441-37-2 | alpha-Methylstyrene - styrene, copolymer, hydrogenated | 3 | SML = 5 mg/kg |  |
| 66960 | 068441-38-3 | alpha-Methylstyrene - vinyltoluene, copolymer, hydrogenated | 3 | SML = 5 mg/kg |  |
| 67120 | 012001-26-2 | Mica | 3 |  |  |
| 67680 | 027107-89-7 | Mono-n-octyltin tris(2-ethylhexyl mercaptoacetate) | 2 | SML(T) = 1.2 mg/kg (18) (as Sn) | 0.02 (Sn) |
| 67840 | - | Montanic acids and/or their esters with ethyleneglycol and/or with 1,3-butanediol and/or with glycerol | 3 |  |  |
| 67850 | 008002-53-7 | Montan wax | 3 |  |  |
| 67891 | 000544-63-8 | Myristic acid | 1 |  | NS |
| 68078 | 027253-31-2 | Neodecanoic acid, cobalt salt | 3 | SML(T) = 0.05 mg/kg (as neodecanoic acid) and SML(T) = 0.05 mg/kg (14) (as Co).Not for use in polymers contacting foods for which simulant D is laid down in Directive 85/572/EEC |  |
| 68140 | 007697-37-2 | Nitric acid | 2 |  | 3 |
| 68145 | 080410-33-9 | 2,2',2"-Nitrilo[triethyl tris(3,3',5,5'-tetra-tert-butyl-1,1'-biphenyl-2,2'-diyl)phosphite] | 3 | SML = 5 mg/kg (sum of phosphite and phosphate) |  |
| 68320 | 002082-79-3 | Octadecyl 3-(3,5-di-tert-butyl-4-hydroxyphenyl)propionate | 2 | SML = 6 mg/kg | 0,1 |
| 68650 | 006700-85-2 | n-Octanoic acid, cobalt salt | 3 | SML(T) = 0.05 mg/kg (14) (as Co) |  |
| 68680 | 016577-52-9 | n-Octanoic acid, lithium salt | 2 | SML(T) = 0.6 mg/kg (8) (as Li) | 0.01 (as Li) |
| 68690 | 006535-19-9 | n-Octanoic acid, manganese salt | 2 | SML(T) = 0.6 mg/kg (10) (as Mn) | 0.01 (as Mn) |
| 68860 | 004724-48-5 | n-Octylphosphonic acid | 3 | SML = 0.05 mg/kg |  |
| 68960 | 000301-02-0 | Oleamide | 3 |  |  |
| 69040 | 000112-80-1 | Oleic acid | 1 |  | NS |
| 69760 | 000143-28-2 | Oleyl alcohol | 3 |  |  |
| 69920 | 000144-62-7 | Oxalic acid | 2 | SML(T) = 6 mg/kg (29) | 0,1 |
| 70240 | 012198-93-5 | Ozokerite | 3 |  |  |
| 70400 | 000057-10-3 | Palmitic acid | 1 |  | NS |
| 71600 | 000115-77-5 | Pentaerythritol | 2 |  | 1 |
| 71680 | 006683-19-8 | Pentaerythritol tetrakis[3-(3,5-di-tert-butyl-4-hydroxyphenyl)propionate] | 2 |  | 3 |
| 71960 | 003825-26-1 | Perfluorooctanoic acid, ammonium salt | 3 |  |  |
| 72081/10 | - | Petroleum hydrocarbon resins (hydrogenated) | 3 | In compliance with the specifications laid down in Annex |  |
| 72640 | 007664-38-2 | Phosphoric acid | 1 |  | 70 (as P) |
| 72800 | 001241-94-7 | Phosphoric acid, diphenyl 2-ethylhexyl ester | 2 | SML = 2.4 mg/kg | 0,04 |
| 73160 | - | Phosphoric acid, mono- and di-n-alkyl(C16 and C18) esters | 3 | SML = 0.05 mg/kg |  |
| 73720 | 000115-96-8 | Phosphoric acid, trichloroethyl ester | 4A | SML = ND (DL= 0.02 mg/kg, analytical tolerance included) |  |
| 74010 | 145650-60-8 | Phosphorous acid, bis(2,4-di-tert-butyl-6-methylphenyl) ethyl ester | 3 | SML = 5 mg/kg (sum of phosphite and phosphate) |  |
| 74240 | 031570-04-4 | Phosphorous acid, tris(2,4-di-tert-butylphenyl) ester | 2 |  | 1 |
| 74400 | - | Phosphorous acid, tris(nonyl- and/or dinonylphenyl) ester | 2 | SML = 30 mg/kg | 0,5 |

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| --- | --- | --- | --- | --- | --- |
| 4560 | 000085-68-7 | Phthalic acid, benzyl butyl ester | 2 | To be used only as: (a) plasticizer in repeated use materials; (b) plasticizer in single-use materials contacing non-fatty foods except for infant formulae as defined by Directive 91/321/EEC and products according to Directive 96/5/EC; (c) technical support agent in concentrations up to 0.1 % in the final product. SML = 30 mg/kg food simulant | ? |
| 74640 | 000117-81-7 | Phthalic acid, bis(2-ethylhexyl) ester | 2 | To be used only as: (a) plasticizer in repeated use materials contacting non-fatty foods; (b) technical support agent in concentrations up to 0.1 % in the final product SML = 1.5 mg/kg food simulant | 0,05 |
| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| 74880 | 000084-74-2 | Phthalic acid, dibutyl ester | 2 | To be used only as: (a) plasticizer in repeated use materials contacting non-fatty foods; (b) technical support agent in concentrations up to 0.05 % in the final product SML = 0.3 mg/kg food simulant | ? |
| 75100 | 068515-48-0 028553-12-0 | Phthalic acid, diesters with primary, saturated C8-C10 branched alcohols, more than 60% C9 | 2 | To be used only as: (a) plasticizer in repeated use materials; (b) plasticizer in single-use materials contacing non-fatty foods except for infant formulae as defined by Directive 91/321/EEC and products according to Directive 96/5/EC; (c) technical support agent in concentrations up to 0.1 % in the final product SML(T) = 9 mg/kg food simulant (42) | ? |

?

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| --- | --- | --- | --- | --- | --- |
| 75105 | 068515-49-1 026761-40-0 | Phthalic acid, diesters with primary, saturated C9-C11 branched alcohols, more than 90% C10 | 2 | To be used only as: (a) plasticizer in repeated use materials; (b) plasticizer in single-use materials contacing non-fatty foods except for infant formulae as defined by Directive 91/321/EEC and products according to Directive 96/5/EC; (c) technical support agent in concentrations up to 0.1 % in the final product SML(T) = 9 mg/kg food simulant (42) | ? |
| 76320 | 000085-44-9 | Phthalic anhydride | 2 |  | 1 |
| 76463 | - | Polyacrylic acid, salts | 3 | SML(T) = 6 mg/kg (36) (for acrylic acid) |  |
| 76681 | 068132-00-3 | Polycyclopentadiene, hydrogenated | 3 | SML = 5 mg/kg (1) |  |
| 76721 | 009016-00-6 063148-62-9 | Polydimethylsiloxane (Mw > 6800) | 2 | In compliance with the specifications laid down in Annex | 1,5 |
| 76723 | 167883-16-1 | Polydimethylsiloxane, 3-aminopropyl terminated, polymer with dicyclohexylmethane-4,4’-diisocyanate | 3 | In compliance with the specifications laid down in Annex. |  |

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| --- | --- | --- | --- | --- | --- |
| 76725 | 661476-41-1 | Polydimethylsiloxane, 3-aminopropyl terminated, polymer with 1-isocyanato—3-isocyanatomethyl-3,5,5-trimethylcyclohexane | 3 | In compliance with the specifications laid down in Annex. |  |
| 76730 | - | Polydimethylsiloxane, gamma-hydroxypropylated | 2 | SML = 6 mg/kg | 0.1 |
| 76866 | - | Polyesters of 1,2-propanediol and/or 1,3- and/or 1,4-butanediol and/or polypropyl- eneglycol with adipic acid, which may be end-capped with acetic acid or fatty acids C12-C18 or n-octanol and/or n-decanol | 2 | SML = 30 mg/kg | 0.5 |
| 76960 | 025322-68-3 | Polyethyleneglycol | 2 |  | 5 |
| 77520 | 061791-12-6 | Polyethyleneglycol ester of castor oil | 2 | SML = 42 mg/kg | 0,7 |
| 77600 | 061788-85-0 | Polyethyleneglycol ester of hydrogenated castor oil | 3 |  |  |
| 77660 | - | Polyethyleneglycol esters of natural fatty acids | 2 |  | 10 |
| 77702 | - | Polyethyleneglycol esters of aliphatic monocarboxylic acids (C6-C22) and their ammonium and sodium sulphates | 2 |  | 10 |
| 77708 | - | Polyethyleneglycol (EO = 1-50) ethers of linear and branched primary alcohols (C8-C22) | 2 | SML = 1.8 mg/kg | 0.03 |
| 77895 | 068439-49-6 | Polyethyleneglycol (EO = 2-6) monoalkyl(C16-C18) ether | 3 | SML = 0.05 mg/kg and in compliance with the specifi-cations laid down in Annex |  |
| 77897 | - | Polyethyleneglycol (EO = 1-50) monoalkyl ether (linear and branched, C8-C20) sulphate, sodium salt | 3 | SML = 5 mg/kg |  |
| 78320 | 009004-97-1 | Polyethyleneglycol monoricinoleate | 2 | SML = 42 mg/kg | 0.7 |
| 79040 | 009005-64-5 | Polyethyleneglycol sorbitan monolaurate | 1 |  | 10 |
| 79120 | 009005-65-6 | Polyethyleneglycol sorbitan monooleate | 2 |  | 10 |
| 79200 | 009005-66-7 | Polyethyleneglycol sorbitan monopalmitate | 1 |  | 10 |
| 79280 | 009005-67-8 | Polyethyleneglycol sorbitan monostearate | 1 |  | 10 |
| 79360 | 009005-70-3 | Polyethyleneglycol sorbitan trioleate | 2 |  | 10 |
| 79440 | 009005-71-4 | Polyethyleneglycol sorbitan tristearate | 1 |  | 10 |
| 79550 | 009014-85-1 | Polyethyleneglycol 2,4,7,9-tetramethyl-5-decyn-4,7-diol ether | 3 |  |  |

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| --- | --- | --- | --- | --- | --- |
| 79600 | 009046-01-9 | Polyethyleneglycol tridecyl ether phosphate | 3 | SML = 5 mg/kg. For materials intended for contact with aqueous foods only. In compliance with the specifica- tions laid down in Annex |  |
| 79920 | 009003-11-6 106392-12-5 | Poly(ethylene propylene)glycol | 3 |  |  |
| 80000 | 009002-88-4 | Polyethylene wax | 3 |  |  |
| 80077 | 068441-17-8 | Polyethylene, oxidized | 7 | In compliance with the specifications of food additive E914 |  |
| 80240 | 029894-35-7 | Polyglycerol ricinoleate | 1 |  | 7.5 |
| 80480 | 090751-07-8 | Poly(6-morpholino-1,3,5-triazine-2,4-diyl)-[(2,2,6,6-tetramethyl-4-piperidyl)-imino]-hexamethylene-[(2,2,6,6-tetramethyl-4-piperidyl)-imino- | 3 | SML = 5 mg/kg and in compliance with the specifications laid down in Annex. |  |
| 80640 | - | Polyoxyalkyl(C2-C4)dimethylpolysiloxane | 3 |  |  |
| 80720 | 008017-16-1 | Polyphosphoric acids | 1 |  | 70 (as P) |
| 80800 | 025322-69-4 | Polypropyleneglycol | 3 |  |  |
| 81060 | 009003-07-0 | Polypropylene wax | 3 |  |  |
| 81200 | 071878-19-8 | Poly[6-[(1,1,3,3-tetramethylbutyl)amino]-1,3,5-triazine-2,4-diyl]-[(2,2,6,6-tetra- methyl-4-piperidyl)-imino]hexamethylene[(2,2,6,6-tetramethyl-4-piperidyl)imino] | 2 | SML = 3 mg/kg | 0.05 |
| 81220 | 192268-64-7 | Poly[[6-[N-(2,2,6,6-tetramethyl-4-piperidinyl)-n-butylamino]-1,3,5-triazine-2,4-diyl]- [2,2,6,6-tetramethyl-4-piperidinyl)imino]-1,6-hexanediyl[(2,2,6,6-tetramethyl-4- piperidinyl)imino]]-alpha-[N,N,N',N'-tetrabutyl-N"-(2,2,6,6-tetramethyl-4-piperidinyl)- N"-(2,2,6,6-tetramethyl-4-piperidinyl)-N"-[6-(2,2,6,6-tetramethyl-4-piperidinylamino)- hexyl][1,3,5-triazine-2,4,6-triamine]-omega-N,N,N',N'-tetrabutyl-1,3,5-triazine- 2,4-diamine] | 3 | SML = 5 mg/kg |  |

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| --- | --- | --- | --- | --- | --- |
| 81280 | 009002-89-5 | Polyvinyl alcohol | 3 | In compliance with the specification laid down in Annex. |  |
| 81500 | 009003-39-8 | Polyvinylpyrrolidone | 3 | In compliance with the specifications laid down in Annex |  |
| 81515 | 087189-25-1 | Poly(zinc glycerolate) | 2-3 | SML(T) = 25 mg/kg (38) (as Zn) |  |
| 81600 | 001310-58-3 | Potassium hydroxide | 1 |  | NS |
| 81680 | 007681-11-0 | Potassium iodide | 1 | SML(T) = 1 mg/kg (11) (as I) | 0.017 (as I) |
| 81840 | 000057-55-6 | 1,2-Propanediol | 1 |  | 25 |
| 81880 | 000071-23-8 | 1-Propanol | 3 |  |  |
| 81882 | 000067-63-0 | 2-Propanol | 1 |  | 1,5 |
| 82000 | 000079-09-4 | Propionic acid | 1 |  | NS |
| 82720 | 006182-11-2 | 1,2-Propyleneglycol distearate | 1 |  | 25 |
| (24010) | 000075-56-9 | Propylene oxide | 4A | QM = 1 mg/kg in FP |  |
| 83440 | 002466-09-3 | Pyrophosphoric acid | 1 |  | 70 |
| 83470 | 014808-60-7 | Quartz | 3 |  |  |
| 83580/1 | 008002-13-9 | Rapeseed oil | 3 |  |  |
| 83595 | 119345-01-6 | Reaction product of di-tert-butyl phosphonite with biphenyl, obtained by condensa-tion of 2,4-di-tert-butylphenol with Friedel Craft reaction product of phosphorus trichloride and biphenyl | 2 | SML = 18 mg/kg and in compliance with the specifica- tions mentioned in Annex | 0.3 |
| 83650 | 009008-34-8 | Resin acids and rosin acids, manganese salts | 2 | SML(T) = 0.6 mg/kg (10) (as Mn) | 0.01 (as Mn) |
| 83700 | 000141-22-0 | Ricinoleic acid | 3 | SML = 42 mg/kg |  |
| 84000 | 008050-31-5 | Rosin, ester with glycerol | 1 |  | 12,5 |
| 84080 | 008050-26-8 | Rosin, ester with pentaerythritol | 2 |  | 1 |
| 84210 | 065997-06-0 | Rosin, hydrogenated | 2 |  | 1 |
| 84240 | 065997-13-9 | Rosin, hydrogenated, ester with glycerol | 3 |  |  |
| 84400 | 064365-17-9 | Rosin, hydrogenated, ester with pentaerythritol | 2 |  | 1 |
| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| 84800 | 000087-18-3 | Salicylic acid, 4-tert-butylphenyl ester | 2 | SML = 12 mg/kg | 0,2 |
| 84880 | 000119-36-8 | Salicylic acid, methyl ester | 1 | SML = 30 mg/kg | 0,5 |
| 85030 | 000111-20-6 | Sebacic acid | 2 |  | 3 |
| 85360 | 000109-43-3 | Sebacic acid, dibutyl ester | 3 |  |  |
| 85550 | 009000-59-3 | Shellac | 1 |  |  |
| 85601 | - | Silicates, natural (with the exception of asbestos) | 3 |  |  |
| 85610 | - | Silicates, natural, silanated (with the exception of asbestos) | 3 |  |  |
| 85680 | 001343-98-2 | Silicic acid | 2 |  | NS |
| 86000 | - | Silicic acid, silanated | 3 |  |  |
| 86160 | 000409-21-2 | Silicon carbide | 3 |  |  |
| 86240 | 007631-86-9 | Silicon dioxide | 1 |  | NS |
| 86285 | - | Silicon dioxide, silanated | 3 |  |  |
| 86440 |  | Sodium aluminate | 2 |  | 1 (as Al) |
| 86480 | 007631-90-5 | Sodium bisulphite | 1 | SML(T) = 10 mg/kg (30) (as SO2) | 0,7 |
| 86720 | 001310-73-2 | Sodium hydroxide | 1 |  | NS |
| 86880 | - | Sodium monoalkyl dialkylphenoxybenzenedisulphonate | 2 | SML = 9 mg/kg | 0,15 |
| 86920 | 007632-00-0 | Sodium nitrite | 3 | SML = 0.6 mg/kg |  |
| 86960 | 007757-83-7 | Sodium sulphite | 1 | SML(T) = 10 mg/kg (30) (as SO2) | 0.7 |
| 87040 | 001330-43-4 | Sodium tetraborate | 2 | SML(T) = 6 mg/kg (23) (as B) without prejudice to the provisions of Directive 98/83/EC on water for human consumption | 0.1 (as B) |
| 87200 | 000110-44-1 | Sorbic acid | 1 |  | 25 |
| 87280 | 029116-98-1 | Sorbitan dioleate | 2 |  | 5 |
| 87520 | 062568-11-0 | Sorbitan monobehenate | 2 |  | 5 |
| 87600 | 001338-39-2 | Sorbitan monolaurate | 1 |  | 5 |
| 87680 | 001338-43-8 | Sorbitan monooleate | 1 |  | 5 |
| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| 87760 | 026266-57-9 | Sorbitan monopalmitate | 1 |  | 25 |
| 87840 | 001338-41-6 | Sorbitan monostearate | 1 |  | 25 |
| 87920 | 061752-68-9 | Sorbitan tetrastearate | 2 |  | 5 |
| 88080 | 026266-58-0 | Sorbitan trioleate | 2 |  | 5 |
| 88160 | 054140-20-4 | Sorbitan tripalmitate | 2 |  | 5 |
| 88240 | 026658-19-5 | Sorbitan tristearate | 1 |  | 25 |
| 88320 | 000050-70-4 | Sorbitol | 1 |  |  |
| 88600 | 026836-47-5 | Sorbitol monostearate | 2 |  | NS |
| 88630/1 | 008001-22-7 | Soybean oil | 3 |  |  |
| 88640 | 008013-07-8 | Soybean oil, epoxidized | 2 | SML = 60 mg/kg. However in the case of PVC gaskets used to seal glass jars con- taining infant formulae and follow-on formulae as defined by Directive 91/321/EEC or containing processed cereal-based foods and baby foods for infants and young children as defined by Directive 96/5/EC, the SML is lowered to 30 mg/kg. In compliance with the specifications laid down in Annex | 1 |

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| --- | --- | --- | --- | --- | --- |
| - | 009045-28-7 | Starch acetate | - | In compliance with the specifications of food additive E1420 | ACC |
| 88800 | 009005-25-8 | Starch, edible | 0 |  |  |
| 88880 | 068412-29-3 | Starch, hydrolysed | 0 |  |  |
| - | 066829-29-6 | Starch octenylsuccinate, sodium salt | - | In compliance with the specifications of food additive E1450 | NS |
| - | 065996-62-5 | Starch, oxidized | - | In compliance with the specifications of food additive E1404 | ACC |
| - | 011120-02-8 | Starch phosphate | - | In compliance with the specifications of food additive E1410 | ACC |
| 88960 | 000124-26-5 | Stearamide | 3 |  |  |
| 89040 | 000057-11-4 | Stearic acid | 1 |  | NS |
| 89120 | 000123-95-5 | Stearic acid, butyl ester | 3 |  |  |
| 89440 | - | Stearic acid, esters with ethyleneglycol | 2 | SML(T) = 30 mg/kg (3) | 0.5 |
| 90720 | 005844-52-9 | Stearoylbenzoylmethane | 2 |  | 1,5 |
| 91200 | 000126-13-6 | Sucrose acetate isobutyrate | 1 |  | 10 |
| 91920 | 007664-93-9 | Sulphuric acid | 1 |  | NS |
| 92000 | 007727-43-7 | Sulphuric acid, barium salt | 3 | SML(T) = 1 mg/kg (12) (as Ba) |  |
| 92030 | 010124-44-4 | Sulphuric acid, copper salt | 2 | SML(T) = 5 mg/kg (7) (as Cu) |  |
| 92080 | 014807-96-6 | Talc | 1 |  | NS |
| 92100 | 061789-97-7 | Tallow | 3 |  |  |
| 92160 | 000087-69-4 | Tartaric acid | 1 |  | 30 |
| 92640 | 000102-60-3 | N,N,N',N'-Tetrakis(2-hydroxypropyl)ethylenediamine | 2 |  | 1 |
| 92700 | 078301-43-6 | 2,2,4,4-Tetramethyl-20-(2,3-epoxypropyl)-7-oxa-3,20-diazadispiro[5.1.11.2]henei- cosan-21-one, polymer | 3 | SML = 5 mg/kg |  |
| 92880 | 041484-35-9 | Thiodiethanolbis[3-(3,5-di-tert-butyl-4-hydroxyphenyl) propionate] | 2 | SML = 2.4 mg/kg | 0.04 |

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| --- | --- | --- | --- | --- | --- |
| 93120 | 000123-28-4 | Thiodipropionic acid, didodecyl ester | 3 | SML(T) = 5 mg/kg (21) |  |
| 93280 | 000693-36-7 | Thiodipropionic acid, dioctadecyl ester | 3 | SML(T) = 5 mg/kg (21) |  |
| 93420 | 007646-78-8 | Tin(IV) chloride | 1 |  | 2 |
| 93440 | 013463-67-7 | Titanium dioxide | 1 |  |  |
| 93540 | 000108-88-3 | Toluene | 3 | SML = 1.2 mg/kg |  |
| 93720 | 000108-78-1 | 2,4,6-Triamino-1,3,5-triazine | 2 | SML = 30 mg/kg | 0,5 |
| 93760 | 000077-90-7 | Tri-n-butyl acetylcitrate |  |  |  |
| 94000 | 000102-71-6 | Triethanolamine | 3 | SML = 0.05 mg/kg |  |
| 94320 | 000112-27-6 | Triethyleneglycol | 2 |  | 5 |
| 94400 | 036443-68-2 | Triethyleneglycol bis[3-(3-tert-butyl-4-hydroxy-5-methylphenyl) propionate] | 2 | SML = 9 mg/kg | 0.15 |
| 94560 | 000122-20-3 | Triisopropanolamine | 3 | SML = 5 mg/kg |  |
| 94960 | 000077-99-6 | 1,1,1-Trimethylolpropane | 2 | SML = 6 mg/kg | 0,1 |
| 95200 | 001709-70-2 | 1,3,5-Trimethyl-2,4,6-tris(3,5-di-tert-butyl-4-hydroxybenzyl)benzene | 2 |  | 1 |
| 95280 | 040601-76-1 | 1,3,5-Tris(4-tert-butyl-3-hydroxy-2,6-dimethylbenzyl)-1,3,5-triazine-2,4,6(1H,3H,5H)- trione | 2 | SML = 6 mg/jg | 0.1 |
| 95360 | 027676-62-6 | 1,3,5-Tris(3,5-di-tert-butyl-4-hydroxybenzyl)-1,3,5-triazine-2,4,6(1H,3H,5H)-trione | 3 | SML = 5 mg/kg |  |
| 95630 | 000057-13-6 | Urea | 0 |  |  |
| 95810 | 000088-12-0 | Vinylpyrrolinone | 4A | SML = ND (DL = 0.01 mg/kg) |  |
| 95855 | 007732-18-5 | Water | 0 | In compliance with Directive 98/83/EC |  |
| 95858 | - | Waxes, paraffinic, refined, derived from petroleum based or synthetic hydrocarbon feedstocks | 3 | SML = 0.05 mg/kg and in compliance with the specifications laid down in Annex. Not to be used for coatings contacting fatty foods. |  |
| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS | ADI/TDI mg/kg bw |
| 95859 | - | Waxes, refined, derived from petroleum based or synthetic hydrocarbon feedstocks | 2 | In compliance with the specifications laid down in Annex | 20 |
| 95870 | - | Wheat protein | 0 |  |  |
| 95883 | - | White mineral oils, paraffinic, derived from petroleum based hydrocarbon feedstocks | 2 | In compliance with the specifications laid down in Annex | 4 |
| 95905 | 013983-17-0 | Wollastonite | 3 |  |  |
| 95935 | 011138-66-2 | Xanthan gum | 1 |  | NS |
| 95945 | 001330-20-7 | Xylene | 3 | SML = 1.2 mg/kg | 0,02 |
| 96180 | - | Zinc dust | 2 | SML(T) = 25 mg/kg (38) (as Zn) |  |
| 96190 | 020427-58-1 | Zinc hydroxide | 2 | SML(T) = 25 mg/kg (38) (as Zn) |  |
| 96200 | 055799-16-1 | Zinc hydroxyphosphite | 2-3 | SML(T) = 25 mg/kg (38) (as Zn) |  |
| 96240 | 001314-13-2 | Zinc oxide | 2 | SML(T) = 25 mg/kg (38) (as Zn) |  |
| 96320 | 001314-98-3 | Zinc sulphide | 2 | SML(T) = 25 mg/kg (38) (as Zn) |  |

D. TEMPORARY APPENDIX TO LIST 1 OF ADDITIVES February 2009

| PM/REF No | CAS No | NAME | SCF-L | RESTRICTIONS AND/OR SPECIFICATIONS |
| --- | --- | --- | --- | --- |
| - | 000071-48-7 | Acetic acid, cobalt(II) salt | - | To be fixed |
| 30100 | 000111-55-7 | Acetic acid, diester with ethyleneglycol | 7 | To be fixed |
| - | 000079-20-9 | Acetic acid, methyl ester | - | To be fixed |
| 30245 | 000109-60-4 | Acetic acid, propyl ester | 7 | To be fixed |
| - | 001118-84-9 | Acetylacetic acid, allyl ester | - | To be fixed |
| 30350 | 000141-97-9 | Acetylacetic acid, ethyl ester | 7 | To be fixed |
| 31330 | - | Acids, fatty, from animal or vegetable fats and oils, methyl esters | 9 | To be fixed |
| - | 091050-89-4 | Acids, fatty (C8-C10), triesters with trimethylolpropane | - | To be fixed |
| - | 085566-27-4 | Acids, fatty (C12-C16), methyl esters | - | To be fixed |
| - | 085865-69-6 | Acids, fatty (C16-C18), isobutyl esters | - | To be fixed |
| - | 085049-37-2 | Acids, fatty (C16-C18 and C18 unsaturated), 2-ethylhexyl esters | - | To be fixed |
| - | 067762-38-3 | Acids, fatty (C16-C18 and C18 unsaturated), methyl esters | - | To be fixed |
| - | 211450-54-3 | Acids, fatty (C16-C18 and C18 unsaturated), methyl esters, epoxidized, reaction products with ethyleneglycol | - | To be fixed |
| - | 068647-95-0 | Acids, fatty, unsaturated (C18), dimers, compounds with coco alkylamines | - | To be fixed |
| - | 147853-32-5 | Acids, fatty, unsaturated (C18), dimers, dimethyl esters, hydrogenated | - | To be fixed |
| - | 048076-38-6 | Acrylic acid, eicosyl ester | - | To be fixed |
| - | 025135-39-1 | Acrylic acid-ethyl acrylate-methyl methacrylate, copolymer | - | To be fixed |
| - | 009010-77-9 | Acrylic acid-ethylene, copolymer | - | To be fixed |
| - | 027515-34-0 | Acrylic acid-ethylene, copolymer, potassium salt | - | To be fixed |
| 31560 | 025085-34-1 | Acrylic acid-styrene, copolymer | D | To be fixed |
| - | 009010-81-5 | Acrylonitrile-butadiene-methacrylic acid, copolymer | - | To be fixed |
| 32480 | 000141-04-8 | Adipic acid, diisobutyl ester | 6B | To be fixed |
| 32760 | 000627-93-0 | Adipic acid, dimethyl ester | 6B | To be fixed |
| - | 068130-33-6 | Adipic acid-pentaerythritol oleate, copolymer | - | To be fixed |
| - | 068002-94-8 | Alcohols, C16-C18 and C18 unsaturated | - | To be fixed |
| - | 085186-55-6 | Alcohols, soya, reaction products with dimethylaminoethanol and maleic anhydride | - | To be fixed |
| - | 068439-57-6 | alpha-Alkene(C14-C16)sulphonic acid, sodium salt | - | To be fixed |
| 33680 | - | Alkyl(C8-C22)arylsulphonic acid | 9 | To be fixed |
| 34165 | - | Alkyl(C8-C18)phenoxybenzenedisulphonic acid, salts | 9 | To be fixed |
| - | 085711-69-9 | Alkyl(C13-C17-sec)sulphonic acid, sodium salts | - | To be fixed |
| - | 085711-70-2 | Alkyl(C14-C18-sec)sulphonic acid, sodium salts | - | To be fixed |
| 34275 | - | Alkyl(C12-C14)sulphuric acid, salts | 9 | To be fixed |
| - | 073296-89-6 | Alkyl(C12-C16)sulphuric acid, sodium salts | - | To be fixed |
| - | 015306-17-9 | Aluminium tris(ethyl acetylacetate) | - | To be fixed |
| - | 095009-16-8 | Amides, from ethylenediamine, oleic acid, stearic acid and vegetable oil fatty acids | - | To be fixed |
| - | 068155-17-9 | Amides, from tall-oil fatty acids and tetraethylenepentamine | - | To be fixed |
| - | 017671-27-1 | Behenic acid, docosyl ester | - | To be fixed |
| - | 025036-25-3 | 2,2-Bis(4-hydroxyphenyl)propane - 2,2-bis(4-hydroxyphenyl)propane bis(2,3-epoxy- propyl) ether, copolymer | - | To be fixed |
| 39730 | 025068-38-6 | 2,2-Bis(4-hydroxyphenyl)propane - epichlorohydrin, copolymer | 9 | To be fixed |
| - | 193098-40-7 | N,N'-Bis(2,2,6,6-tetramethyl-4-piperidyl)hexamethylenediamine, polymers with morpholine-2,4,6-trichloro-1,3,5-triazine reaction products, methylated | - | To be fixed |
| - | 030007-47-7 | 5-Bromo-5-nitro-1,3-dioxane | - | To be fixed |
| 40460 | 000052-51-7 | 2-Bromo-2-nitro-1,3-propanediol | 8 | To be fixed |
| 40592 | 000078-92-2 | 2-Butanol | 8 | To be fixed |
| 40618 | 005131-66-8 | 1-Butoxy-2-propanol | 8 | To be fixed |
| - | 025767-47-9 | Butyl acrylate-styrene, copolymer | - | To be fixed |
| - | 000075-91-2 | tert-Butyl hydroperoxide | - | To be fixed |
| - | 009011-53-4 | Butyl methacrylate-isobutyl methacrylate, copolymer | - | To be fixed |
| - | 025608-33-7 | Butyl methacrylate-methyl methacrylate, copolymer | - | To be fixed |
| 40840 | 001638-22-8 | 4-Butylphenol | 8 | To be fixed |
| - | 002273-43-0 | Butylstannoic acid | - | To be fixed |
| 41000 | 000096-48-0 | gamma-Butyrolactone | 8 | To be fixed |
| - | 025950-96-3 | Carbonic acid, polyester with 1,4-butanediol | - | To be fixed |
| - | 085361-59-0 | Castor oil, epoxidized, sulphated, ammonium salt | - | To be fixed |
| - | 211450-53-2 | Castor oil fatty acids, methyl esters, reaction products with 1,3-bis(1-isocyanato- 1-methylethyl)benzene, polyethyleneglycol, polyethyleneglycol monooctyl ether and trimethylolpropane | - | To be fixed |
| - | 211450-52-1 | Castor oil fatty acids, methyl esters, reaction products with 1,3-bis(1-isocyanato- 1-methylethyl)benzene, polyethyleneglycol, propyleneglycol and trimethylolpropane | - | To be fixed |
| 43230 | 008002-33-3 | Castor oil, sulphated | 9 | To be fixed |
| - | 068187-77-9 | Castor oil, sulphated, ammonium salt | - | To be fixed |
| - | 068187-76-8 | Castor oil, sulphated, sodium salt | - | To be fixed |
| - | 003811-04-9 | Chloric acid, potassium salt | - | To be fixed |
| - | 000079-07-2 | Chloroacetamide | - | To be fixed |
| 43630 | 000059-50-7 | p-Chloro-m-cresol | 8 | To be fixed |
| 43760 | 026172-55-4 | 5-Chloro-2-methyl-4-isothiazolin-3-one | 7 | To be fixed |
| - | 001308-38-9 | Chromium(III) oxide | - | To be fixed |
| 44560 | 000077-94-1 | Citric acid, tributyl ester | 6B | To be fixed |
| - | 061788-46-3 | Cocoalkylamines | - | To be fixed |
| - | 061791-14-8 | Cocoalkylamines, ethoxylated | - | To be fixed |
| - | 061791-63-7 | N-Cocoalkyltrimethylenediamines | - | To be fixed |
| 45040 | 068603-42-9 | Coconut oil fatty acids diethanolamide | 7 | To be fixed |
| 45120 | - | Copolymers of acrylic, fumaric, itaconic, maleic and methacrylic acids with butadiene, butene, divinylbenzene, esters of these acids with saturated mono- hydric alcohols (C1-C18), ethylene, ethylene oxide, etc. | 9 | To be fixed |
| 45710 | 000108-93-0 | Cyclohexanol | 8 | To be fixed |
| 45720 | 000108-94-1 | Cyclohexanone | 6A | To be fixed |
| 45730 | 025054-06-2 | Cyclohexanone-formaldehyde, copolymer | 9 | To be fixed |
| - | 000091-17-8 | Decahydronaphthalene | - | To be fixed |
| 46440 | 000094-36-0 | Dibenzoyl peroxide | 8 | To be fixed |
| - | 000088-58-4 | 2,5-Di-tert-butylhydroquinone | - | To be fixed |
| 47040 | 034137-09-2 | 3,5-Di-tert-butyl-4-hydroxyhydrocinnamic acid, triester with 1,3,5-tris(2-hydroxy- ethyl)-1,3,5-triazine-2,4,6(1H,3H,5H)-trione | 8 | To be fixed |
| - | 000683-18-1 | Dibutyltin dichloride | - | To be fixed |
| 47220 | 000077-58-7 | Dibutyltin dilaurate | 8 | To be fixed |
| - | 068611-44-9 | Dichlorodimethylsilane, reaction products with silica | - | To be fixed |
| 47620 | 000111-42-2 | Diethanolamine | 8 | To be fixed |
| 47720 | 000120-55-8 | Diethyleneglycol dibenzoate | W | To be fixed |
| - | 000124-17-4 | Diethyleneglycol monobutyl ether acetate | - | To be fixed |
| 48370 | 000100-37-8 | Diethylethanolamine | 8 | To be fixed |
| 49340 | 061789-71-7 | Dimethyl(cocoalkyl)benzylammonium chloride | 9 | To be fixed |
| - | 000112-18-5 | N,N-Dimethyldodecylamine | - | To be fixed |
| 49510 | - | alpha,omega-Dimethylpoly(o-butylpolypropyleneglycol)(polyethyleneglycol)(poly- dimethylsiloxane) | 9 | To be fixed |
| 51160 | 000123-91-1 | Dioxane | 6A | To be fixed |
| 51870 | 034590-94-8 | Dipropyleneglycol monomethyl ether | 8 | To be fixed |
| - | 064742-52-5 | Distillates (petroleum), hydrotreated heavy naphthenic | - | To be fixed |
| - | 064741-88-4 | Distillates (petroleum), solvent-refined heavy paraffinic | - | To be fixed |
| - | 064741-89-5 | Distillates (petroleum), solvent-refined light paraffinic | - | To be fixed |
| - | 068131-89-5 | Distillates (petroleum), steam-cracked, polymers with ethylene-manuf.-by-product piperylene-cut alkenes | - | To be fixed |
| - | 000112-55-0 | n-Dodecylmercaptan | - | To be fixed |
| 52240 | 028519-02-0 | Dodecylphenoxybenzenedisulphonic acid, disodium salt | 8 | To be fixed |
| - | 026376-86-3 | Ethyl acrylate - 2-ethylhexyl acrylate, copolymer | - | To be fixed |
| - | 106990-43-6 | N,N"'-Ethylenebis[N-[3-[[4,6-bis[butyl(1,2,2,6,6-pentamethyl-4-piperidinyl)-amino]- 1,3,5-triazin-2-yl]amino]propyl]-N',N"-dibutyl-N',N"-bis(1,2,2,6,6-pentamethyl-4- piperidinyl)-2,4,6-triamino-1,3,5-triazine | - | To be fixed |
| 53700 | - | Ethyleneglycol-methylsiloxane, copolymer | 9 | To be fixed |
| - | 000122-99-6 | Ethyleneglycol monophenyl ether | - | To be fixed |
| 53900 | 050586-59-9 | Ethyleneglycol-trimethylolpropane, copolymer | 9 | To be fixed |
| - | 025053-53-6 | Ethylene-methacrylic acid, copolymer | - | To be fixed |
| 54060 | 024937-78-8 | Ethylene-vinyl acetate, copolymer | D | To be fixed |
| 54100 | - | Ethylene-vinyl esters of saturated aliphatic monocarboxylic acids (C2-C18), copolymer | 9 | To be fixed |
| 54120 | 000149-57-5 | 2-Ethylhexanoic acid | 6B | To be fixed |
| 54130 | 024593-34-8 | 2-Ethylhexanoic acid, cerium salt | 6B | To be fixed |
| 54140 | 000136-52-7 | 2-Ethylhexanoic acid, cobalt(II) salt | 6B | To be fixed |
| 54190 | 015956-58-8 | 2-Ethylhexanoic acid, manganese salt | 6B | To be fixed |
| - | 000301-10-0 | 2-Ethylhexanoic acid, tin(II) salt | - | To be fixed |
| 54220 | 022464-99-9 | 2-Ethylhexanoic acid, zirconium salt | 6B | To be fixed |
| 54380 | 008047-99-2 | N-Ethyltoluenesulphonamide | 8 | To be fixed |
| 54395 | 035835-94-0 | Ethyltriphenylphosphonium acetate | 8 | To be fixed |
| - | 068526-50-1 | Fatty acids, tallow, isobutyl esters | - | To be fixed |
| 54900 | 009017-33-8 | Formaldehyde-naphthalenesulphonic acid, copolymer | 9 | To be fixed |
| 54960 | 001338-51-8 | Formaldehyde-toluenesulphonamide, copolymer | 9 | To be fixed |
| 58310 | 000107-22-2 | Glyoxal | 6A | To be fixed |
| - | 012173-47-6 | Hectorite | - | To be fixed |
| - | 029316-77-6 | Hexadecyl methacrylate-octadecyl methacrylate, copolymer | - | To be fixed |
| - | 085585-92-8 | Hexanediamide, N,N'-dialkyl(C8-C18) derivatives | - | To be fixed |
| 59520 | 002425-77-6 | 2-Hexyldecanol | 8 | To be fixed |
| 59600 | 000107-41-5 | Hexyleneglycol | 7 | To be fixed |
| - | 267233-58-9 | Hydrocarbon resins, aliphatic | - | To be fixed |
| - | 267233-95-4 | Hydrocarbon resins, aromatic | - | To be fixed |
| - | 267233-62-5 | Hydrocarbon resins, cyclodiene | - | To be fixed |
| - | 267233-74-9 | Hydrocarbon resins, hydrogenated | - | To be fixed |
| - | 002809-21-4 | 1-Hydroxyethanediphosphonic acid | - | To be fixed |
| 60640 | 000150-39-0 | N-(2-Hydroxyethyl)ethylenediaminetriacetic acid | 8 | To be fixed |
| 61340 | 000149-44-0 | Hydroxymethanesulphinic acid, sodium salt | 8 | To be fixed |
| - | 003147-75-9 | 2-[2'-Hydroxy-5'-(1,1,3,3-tetramethylbutyl)phenyl]benzotriazole | - | To be fixed |
| - | 056780-58-6 | 2-Hydroxy-3-(trimethylammonio)propyl starch chloride | - | To be fixed |
| 62110 | 007681-52-9 | Hypochlorous acid, sodium salt | 6A | To be fixed |
| - | 072749-55-4 | Imidazolium compounds, 2-(C17 and C17-unsaturated alkyl)-1-[2-(C18 and C18- unsaturated amino)ethyl]-4,5-dihydro-1-methyl, methyl sulphates | - | To be fixed |
| - | 020344-49-4 | Iron hydroxide oxide | - | To be fixed |
| - | 000089-65-6 | Isoascorbic acid | - | To be fixed |
| 62270 | 000078-83-1 | Isobutanol | 8 | To be fixed |
| - | 006846-50-0 | Isobutyric acid, diester with 2,2,4-trimethyl-1,3-pentanediol | - | To be fixed |
| - | 097259-92-2 | Isononanoic acid, butyl ester | - | To be fixed |
| 62860 | 008008-20-6 | Kerosene | 9 | To be fixed |
| - | 000097-64-3 | Lactic acid, ethyl ester | - | To be fixed |
| - | 037811-72-6 | Lauric acid, isobutyl ester | - | To be fixed |
| - | 010233-13-3 | Lauric acid, isopropyl ester | - | To be fixed |
| 63600 | 000097-78-9 | N-Lauroylsarcosine | 8 | To be fixed |
| 63880 | - | Light petroleum hydrocarbons, odorless | 9 | To be fixed |
| 64240 | 008016-11-3 | Linseed oil, epoxidized (oxirane < 10%, iodine number <6) | 7 | To be fixed |
| - | 001309-38-2 | Magnetite | - | To be fixed |
| - | 000142-16-5 | Maleic acid, bis(2-ethylhexyl) ester | - | To be fixed |
| 64940 | - | Maleic anhydride-ethylene or styrene or methyl vinyl ether, copolymer | 9 | To be fixed |
| 64985 | 025722-45-6 | Maleic anhydride-propylene, copolymer | 9 | To be fixed |
| 65768 | 000149-30-4 | 2-Mercaptobenzothiazole | 6A | To be fixed |
| - | 000109-16-0 | Methacrylic acid, diester with triethyleneglycol | - | To be fixed |
| - | 007779-31-9 | Methacrylic acid, 3,3,5-trimethylcyclohexyl ester | - | To be fixed |
| 66030 | 000150-76-5 | 4-Methoxyphenol | 8 | To be fixed |
| 66320 | 000118-82-1 | 4,4'-Methylenebis(2,6-di-tert-butylphenol) | 8 | To be fixed |
| - | 066204-44-2 | 3,3'-Methylenebis(5-methyloxazolidine) | - | To be fixed |
| 66715 | 000693-98-1 | 2-Methylimidazole | 8 | To be fixed |
| 66820 | 000923-02-4 | N-Methylolmethacrylamide | 7 | To be fixed |
| 66860 | 000108-11-2 | 4-Methyl-2-pentanol | 8 | To be fixed |
| - | 023850-94-4 | Monobutyltin tris(2-ethylhexanoate) | - | To be fixed |
| - | 064742-82-1 | Naphtha(petroleum), hydrodesulphurized heavy | - | To be fixed |
| - | 064742-49-0 | Naphtha(petroleum), hydrotreated light | - | To be fixed |
| - | 001338-24-5 | Naphthenic acids | - | To be fixed |
| - | 061789-36-4 | Naphthenic acids, calcium salts | - | To be fixed |
| 67930 | 061789-51-3 | Naphthenic acids, cobalt salts | 9 | To be fixed |
| - | 001338-02-9 | Naphthenic acids, copper salts | - | To be fixed |
| 67946 | 001336-93-2 | Naphthenic acids, manganese salts | 9 | To be fixed |
| - | 026896-20-8 | Neodecanoic acid | - | To be fixed |
| - | 027253-29-8 | Neodecanoic acid, zinc salt | - | To be fixed |
| - | 005064-31-3 | Nitrilotriacetic acid, trisodium salt | - | To be fixed |
| 68185 | 000104-40-5 | 4-Nonylphenol | 8 | To be fixed |
| 68640 | 007435-02-1 | n-Octanoic acid, cerium salt | 8 | To be fixed |
| 68730 | 018312-04-4 | Octanoic acid, zirconium salt | 9 | To be fixed |
| (22675) | 000111-86-4 | Octylamine | 8 | To be fixed |
| 68775 | 005333-42-6 | 2-Octyldodecanol | 8 | To be fixed |
| 69120 | 000142-77-8 | Oleic acid, butyl ester | 7 | To be fixed |
| - | 026399-02-0 | Oleic acid, 2-ethylhexyl ester | - | To be fixed |
| - | 058353-68-7 | N-Oleylsulphosuccinamic acid, sodium salt | - | To be fixed |
| 71120 | 008012-95-1 | Paraffin oil | 9 | To be fixed |
| 71121 | - | Paraffin oil (hydrogenated) | D | To be fixed |
| 71122 | - | Paraffin oil (conventional) | D | To be fixed |
| - | 068188-18-1 | Paraffin oils, chlorosulphonated, saponified | - | To be fixed |
| 72046 | 007727-54-0 | Persulphuric acid, ammonium salt | 8 | To be fixed |
| 72048 | 007727-21-1 | Persulphuric acid, potassium salt | 8 | To be fixed |
| - | 007775-27-1 | Persulphuric acid, sodium salt | - | To be fixed |
| 72060 | 008009-03-8 | Petrolatum | 9 | To be fixed |
| 72061 | - | Petrolatum (hydrogenated) | D | To be fixed |
| 72135 | 000094-84-2 | Phenothiazine | 8 | To be fixed |
| 72240 | 000132-27-4 | 2-Phenylphenol, sodium salt | D | To be fixed |
| - | 068515-98-0 | Phosphoric acid, alkyl(C3-C9) esters | - | To be fixed |
| - | 000107-66-4 | Phosphoric acid, dibutyl ester | - | To be fixed |
| - | 012645-31-7 | Phosphoric acid, 2-ethylhexyl ester | - | To be fixed |
| - | 001623-15-0 | Phosphoric acid, monobutyl ester | - | To be fixed |
| 73280 | - | Phosphoric acid, mono- and diesters with alcohols, aliphatic (C9-C18), salts | 9 | To be fixed |
| 73600 | 000078-51-3 | Phosphoric acid, tributoxyethyl ester | 6B | To be fixed |
| 73680 | 000126-73-8 | Phosphoric acid, tributyl ester | 6B | To be fixed |
| 73840 | 000126-71-6 | Phosphoric acid, triisobutyl ester | 6B | To be fixed |
| 73920 | 000115-86-6 | Phosphoric acid, triphenyl ester | 6B | To be fixed |
| (23178) | 000101-02-0 | Phosphorous acid, triphenyl ester | 8 | To be fixed |
| 74760 | 027987-25-3 | Phthalic acid, bis(methylcyclohexyl) ester | 8 | To be fixed |
| 74960 | 000084-61-7 | Phthalic acid, dicyclohexyl ester | 7 | To be fixed |
| 75120 | 000084-66-2 | Phthalic acid, diethyl ester | 7 | To be fixed |
| 75280 | 000084-69-5 | Phthalic acid, diisobutyl ester | 6B | To be fixed |
| 75600 | 000131-11-3 | Phthalic acid, dimethyl ester | 6B | To be fixed |
| 75840 | 000117-84-0 | Phthalic acid, di-n-octyl ester | 6B | To be fixed |
| 76005 | 000085-70-1 | Phthalic acid, mixed esters with butyl glycolate and butanol | 7 | To be fixed |
| 76445 | 009003-05-8 | Polyacrylamide | 9 | To be fixed |
| 76461 | 009003-01-4 | Polyacrylic acid | 7 | To be fixed |
| - | 068441-49-6 | Polybutadiene, epoxidized, cyclized | - | To be fixed |
| - | 129288-65-9 | Polybutadiene, epoxidized, hydroxy-terminated | - | To be fixed |
| 76520 | 009003-29-6 | Polybutene | D | To be fixed |
| 76540 | 009003-49-0 | Polybutyl acrylate | 9 | To be fixed |
| - | 026222-20-8 | Polyester of 1,2-propanediol with sebacic acid | - | To be fixed |
| - | - | Polyetherpolyols | - | To be fixed |
| 76980 | 024938-37-2 | Polyethyleneglycol adipate | 7 | To be fixed |
| 77020 | - | Polyethyleneglycol alkyl(C3-C18) ether | 9 | To be fixed |
| - | 125301-88-4 | Polyethyleneglycol alkyl(C12-C14 )ether ammonium sulphate | - | To be fixed |
| - | 068130-47-2 | Polyethyleneglycol alkyl(C8-C10) ether phosphate | - | To be fixed |
| 77030 | 068891-38-3 | Polyethyleneglycol alkyl(C12-C14 )ether sodium sulphate | 9 | To be fixed |
| 77035 | - | Polyethyleneglycol (EO = 2-3)alkyl(C12-C14)ether sodium sulphate | 8 | To be fixed |
| 77070 | 068954-91-6 | Polyethyleneglycol alkyl(C10-C12) ether sulphosuccinate, disodium salt | 9 | To be fixed |
| 77072 | - | Polyethyleneglycol alkyl(C10-C16) ether sulphosuccinate, disodium salt | D | To be fixed |
| - | 009004-82-4 | Polyethyleneglycol dodecyl ether, sodium sulphate | - | To be fixed |
| - | 039354-45-5 | Polyethyleneglycol dodecyl ether sulphosuccinate, disodium salt | - |  |
| - | 009014-92-0 | Polyethyleneglycol dodecylphenyl ether | - | To be fixed |
| 77705 | - | Polyethyleneglycol (> 20 EO) ethers of alkylphenols, sodium sulphates | 9 | To be fixed |
| - | 084133-50-6 | Polyethyleneglycol ethers of C12-C14 secondary alcohols | - | To be fixed |
| 77730 | - | Polyethyleneglycol ethers of alcohols, aliphatic, monohydric, saturated, primary, linear (C5-C15) | 9 | To be fixed |
| 77735 | 059269-54-4 | Polyethyleneglycol ether of dodecylphenol, sodium sulphate | 9 | To be fixed |
| 77747 | - | Polyethyleneglycol ether of octylphenol, sodium sulphate | 9 | To be fixed |
| 77760 | 061791-28-4 | Polyethyleneglycol ether of tallow fatty alcohol | D | To be fixed |
| - | 037205-87-1 | Polyethyleneglycol isononylphenyl ether | - |  |
| 77880 | 009043-30-5 | Polyethyleneglycol isotridecyl ether | 8 | To be fixed |
| 78400 | 009016-45-9 | Polyethyleneglycol nonylphenyl ether | P | To be fixed |
| 78440 | 026027-38-3 | Polyethyleneglycol 4-nonylphenyl ether | W7 | To be fixed |
| - | 009051-57-4 | Polyethyleneglycol nonylphenyl ether, ammonium sulphate | - | To be fixed |
| - | 068412-54-4 | Polyethyleneglycol nonylphenyl ether, branched | - | To be fixed |
| 78460 | 009014-90-8 | Polyethyleneglycol nonylphenyl ether, sodium sulphate | P | To be fixed |
| 78480 | 051811-79-1 | Polyethyleneglycol nonylphenyl phosphate | 9 | To be fixed |
| 78520 | 009040-38-4 067999-57-9 | Polyethyleneglycol nonylphenyl sulphosuccinate, disodium salt | 9 | To be fixed |
| 78560 | 009002-93-1 009036-19-5 | Polyethyleneglycol octylphenyl ether | 9 | To be fixed |
| - | 068649-55-8 | Polyethyleneglycol nonylphenyl ether, branched, ammonium sulphate | - | To be fixed |
| - | 069011-84-3 | Polyethyleneglycol octylphenyl ether, sodium sulphate, branched | - | To be fixed |
| - | 060828-78-6 | Polyethyleneglycol trimethylnonyl ether | - | To be fixed |
| - | 070559-25-0 | Polyethyleneglycol 2,4,6-tristyrylphenyl ether | - | To be fixed |
| - | 127036-24-2 | Polyethyleneglycol undecyl ethers, branched and linear | - | To be fixed |
| 78720 | - | Polyethyleneglycol and/or polypropyleneglycol ethers of aliphatic monohydric alcohols (C8-C20) and their ammonium and sodium sulphates | 9 | To be fixed |
| 78800 | - | Polyethyleneglycol and/or polypropyleneglycol ethers of alkylphenols and their ammonium and sodium sulphates | 9 | To be fixed |
| 79920 | 009003-11-6 | Poly(ethylene propylene)glycol | 7/9 | To be fixed |
| 79930 | - | Poly(ethylene propylene)glycol (>20 EO and >20 PO) | 9 | To be fixed |
| - | 055963-27-4 | Poly(ethylene propylene)glycol dibehenate | - | To be fixed |
| - | 068987-81-5 | Poly(ethylene propylene)glycol ethers of C6-C10 alcohols | - | To be fixed |
| - | 174955-61-4 | Poly(ethylene propylene)glycol ether of 10-(hydroxymethyl)-2-pinene | - | To be fixed |
| - | 061725-89-1 | Poly(ethylene propylene)glycol tridecyl ether | - | To be fixed |
| 80360 | 009003-27-4 | Polyisobutene | 7 | To be fixed |
| 80460 | 025087-26-7 | Polymethacrylic acid | D | To be fixed |
| 80850 | - | Polypropyleneglycol (MW > 1000) butyl ether | 9 | To be fixed |
| 80930 | - | Polypropyleneglycol ether of trimethylolpropane | 9 | To be fixed |
| 80985 | - | Polypropyleneglycol (MW > 1000) oleate butyl ether | 9 | To be fixed |
| 81030 | - | Polypropyleneglycol stearate | 9 | To be fixed |
| 81120 | - | Polyterpenes | 9 | To be fixed |
| 81160 | 009002-84-2 | Polytetrafluoroethylene | D | To be fixed |
| 81260 | - | Polyvinyl acetate, partially hydrolyzed | 7 | To be fixed |
| (23710) | 063148-65-2 | Polyvinylbutyrals | 9 | To be fixed |
| 81310 | 009002-86-2 | Polyvinyl chloride | D | To be fixed |
| 81390 | 025104-37-4 | Poly(vinyl ethyl ether) | 9 | To be fixed |
| 82050 | 000108-32-7 | Propylene carbonate | 8 | To be fixed |
| - | 121888-66-2 | Quaternary ammonium compounds, benzylbis(hydrogenated tallow alkyl)methyl, benzoate lauryl sulphate, salts with bentonite | - | To be fixed |
| 83480 | 121888-67-3 | Quaternary ammonium compounds, benzylbis(hydrogenated tallow alkyl)methyl, bis(hydrogenated tallow alkyl)dimethylammonium salt with hectorite | 9 | To be fixed |
| 83510 | - | Quaternary ammonium compounds, benzyl(hydrogenated tallow alkyl)dimethyl, chlorides, compounds with bentonite and sodium stearate | 9 | To be fixed |
| 83530 | 071011-24-0 | Quaternary ammonium compounds, benzyl(hydrogenated tallow alkyl)dimethyl, chlorides, compounds with bentonite | 9 | To be fixed |
| - | 071011-27-3 | Quaternary ammonium compounds, bis(hydrogenated tallow alkyl)dimethyl, chlorides, compounds with hectorite | - | To be fixed |
| 83560 | 068953-58-2 | Quaternary ammonium compounds, bis(hydrogenated tallow alkyl)dimethyl, salts with bentonite) | 9 | To be fixed |
| - | 085586-25-0 | Rapeseed oil fatty acids, methyl esters | - | To be fixed |
| - | 065997-04-8 | Rosin, fumarated | - | To be fixed |
| - | 068201-58-1 | Rosin, fumarated, polymer with formaldehyde | - | To be fixed |
| - | 065997-11-7 | Rosin, fumarated, polymer with pentaerythritol | - | To be fixed |
| - | 008050-28-0 | Rosin, maleated | - | To be fixed |
| - | 065997-07-1 | Rosin, polymer with formaldehyde | - | To be fixed |
| - | 068475-37-6 | Rosin, polymerised, ester with glycerol | - | To be fixed |
| - | 083137-13-7 | Rosin, reaction products with acrylic acid | - | To be fixed |
| 86050 | 000078-10-4 | Silicic acid, tetraethyl ester | 8 | To be fixed |
| - | 068412-37-3 | Silicic acid, tetraethyl ester, hydrolysed | - | To be fixed |
| 86300 | 063148-62-9 | Silicone oils | 9 | To be fixed |
| - | - | Silicones in compliance with Recommendation XV of the BfR | - | To be fixed |
| 86430 | - | Silver chloride (20% w/w) coated onto titanium dioxide (80% w/w) | 7 | To be fixed |
| 86670 | 007775-14-6 | Sodium dithionite | 8 | To be fixed |
| - | 007681-57-4 | Sodium metabisulphite | - | To be fixed |
| 88680 | 008002-23-1 | Spermaceti wax | 8 | To be fixed |
| - | 009057-06-1 | Starch carboxymethyl ether | - | To be fixed |
| - | 039316-70-6 | Starch succinate | - | To be fixed |
| - | 007047-84-9 | Stearic acid, dihydroxyaluminium salt | - | To be fixed |
| 89520 | 008045-34-9 | Stearic acid, esters with pentaerythritol | 7 | To be fixed |
| 90000 | 000646-13-9 | Stearic acid, isobutyl ester | 7 | To be fixed |
| - | 031565-37-4 | Stearic acid, isotridecyl ester | - | To be fixed |
| - | 007637-13-0 | Stearic acid, tin salt | - | To be fixed |
| 91135 | 000106-65-0 | Succinic acid, dimethyl ester | 7 | To be fixed |
| 91560 | 002373-38-8 | Sulphosuccinic acid, bis(1,3-dimethylbutyl) ester, sodium salt | 6B | To be fixed |
| 91570 | 010041-19-7 | Sulphosuccinic acid, bis(2-ethylhexyl) ester | 6B | To be fixed |
| 91572 | 000577-11-7 | Sulphosuccinic acid, bis(2-ethylhexyl) ester, sodium salt | 6B | To be fixed |
| 91580 | 023386-52-9 | Sulphosuccinic acid, dicyclohexyl ester, sodium salt | 8 | To be fixed |
| 91630 | 003006-15-3 | Sulphosuccinic acid, dihexyl ester, sodium salt | 6B | To be fixed |
| 91665 | 029857-13-4 | Sulphosuccinic acid, diisodecyl ester, sodium salt | 6B | To be fixed |
| 91672 | 055184-72-0 | Sulphosuccinic acid, diisotridecyl ester, sodium salt | 6B | To be fixed |
| 91680 | 001639-66-3 | Sulphosuccinic acid, dioctyl ester, sodium salt | 6B | To be fixed |
| 91720 | 000922-80-5 | Sulphosuccinic acid, dipentyl ester, sodium salt | 6B | To be fixed |
| 91760 | 002673-22-5 | Sulphosuccinic acid, ditridecyl ester, sodium salt | 6B | To be fixed |
| 91800 | 037294-49-8 | Sulphosuccinic acid, isodecyl ester, disodium salt | 8 | To be fixed |
| 92120 | - | Tallow, sulphated, ammonium, potassium or sodium salt | 9 | To be fixed |
| - | 000586-62-9 | Terpinolene | - | To be fixed |
| 92685 | 000126-86-3 | 2,4,7,9-Tetramethyl-5-decyne-4,7-diol | 8 | To be fixed |
| - | 000546-68-9 | Tetraisopropyl titanate | - | To be fixed |
| 93585 | 000104-15-4 | p-Toluenesulphonic acid | 8 | To be fixed |
| - | 004719-04-4 | 1,3,5-triazine-1,3,5(2H,4H,6H)-triethanol | - | To be fixed |
| 93760 | 000077-90-7 | Tributyl acetyl citrate | ? | To be fixed |
| 93790 | 000102-82-9 | Tributylamine | 8 | To be fixed |
| 94240 | 000077-89-4 | Triethyl acetyl citrate | 8 | To be fixed |
| 94270 | 000121-44-8 | Triethylamine | 8 | To be fixed |
| - | 000143-22-6 | Triethyleneglycol monobutyl ether | - | To be fixed |
| 95230 | 000603-35-0 | Triphenylphosphine | 8 | To be fixed |
| 95400 | 000090-72-2 | 2,4,6-Tris[(dimethylamino)methyl]phenol | 8 | To be fixed |
| - | 025213-24-5 | Vinyl acetate-vinyl alcohol, copolymer | - | To be fixed |
| - | 025086-48-0 | Vinyl acetate-vinyl alcohol, vinyl chloride, copolymer | - | To be fixed |
| 95730 | 009003-22-9 | Vinyl acetate-vinyl chloride, copolymer | D | To be fixed |
| - | 009005-09-8 | Vinyl acetate-vinyl chloride-maleic acid, copolymer | - | To be fixed |
| 95755 | 025086-89-9 | Vinyl acetate-vinylpyrrolidone, copolymer | 9 | To be fixed |
| - | 003039-83-6 | Vinylsulphonic acid, sodium salt | - | To be fixed |
| 95880 | 008042-47-5 | White mineral oil | 9 | To be fixed |
| 95881 | - | White mineral oil (hydrogenated) | D | To be fixed |
| 96220 | 000557-09-5 | Zinc octanoate | D | To be fixed |
| 96400 | 053801-45-9 | Zirconium oxide | 7 | To be fixed |
| 96480 | 032535-84-5 | Zirconyl ammonium carbonate | 7 | To be fixed |